| AUSTROADS TECHNICAL SPECIFICATION ATS 5530 Supply of Pot Bearings |  |
| --- | --- |

Contents 1. Scope 2 2. Referenced Documents 2 3. Definitions 4 4. Quality System Requirements 5 5. Design 5 General 5 Design Documentation and Certification 6 6. Materials 7 General 7 Ferrous Materials 7 Sliding Pads and Strips 8 Elastomeric Disc 8 Internal Seals 8 Lubricant 8 Material Conformity 9 7. Fabrication 9 General 9 Flatness of Surfaces 9 Pot 9 Piston 10 External Seal 10 Elastomeric Disc 10 Internal Seal - POM or Carbon Filled PTFE 10 Internal Seal - Brass 10 Stainless Steel Sliding Surface 11 Guide Bars 11 8. Protective Treatment – Structural Steel Bearings 12 General 12 Surface Preparation 13 Zinc Metal Spray 13 Hot-Dip Galvanizing 13 Paint Application 13 9. Protective Treatment – Stainless Steel Bearings 14 General 14 Insulation 14 10. Testing 15 General 15 Geometrical Verification 15 Load Tests 16 Vertical Load Test 16 Lateral Load Test 16 Rotation Test 16 Coefficient of Friction Test 17 Criteria for Acceptance 17 11. Identification and Delivery 18 Annexure A: Summary of Hold Points, Witness Points and Records 19 Annexure B: ZP Coating System 20

# Scope

Austroads Technical Specification ATS 5530 sets out the requirements for the supply of pot bearings and associated attachment plates, including their design and fabrication.  It applies to pot bearings with both structural (i.e., carbon) steel and stainless steel components.

For bearing installation requirements, refer to ATS 5570.

# Referenced Documents

The following documents are referenced in this specification:

Australian / New Zealand Standards AS/NZS 1214 Hot-dip galvanized coatings on threaded fasteners (ISO metric coarse thread series) AS/NZS 1554 Structural steel welding AS/NZS 1554.6 Part 6: Welding stainless steels for structural purposes AS/NZS 1567 Copper and copper alloys – Wrought rods, bars and sections AS 1627 Metal finishing – Preparation and pretreatment of surfaces AS 1627.1 Part 1: Removal of oil, grease and related contamination AS 1627.4 Part 4: Abrasive blast cleaning AS/NZS 2312 Guide to the protection of structural steel against atmospheric corrosion by the use of protective coatings AS/NZS 2312.1 Part 1: Paint coatings AS/NZS 2312.2 Part 2: Hot dip galvanizing AS 2331.1.3 Methods of test for metallic and related coatings: Method 1.3: Local thickness tests – Magnetic method AS 2700 Colour standards for general purposes AS/NZS 3678 Structural steel - Hot-rolled plates, floorplates and slabs AS/NZS 3679.1 Structural steel - Hot-rolled bars and sections AS 3894 Site testing of protective coating AS 3894.3 Part 3: Determination of dry film thickness AS 3894.5 Part 5: Determination of surface profile AS/NZS 4680 Hot-dip galvanized (zinc) coatings on fabricated ferrous articles AS 5100 Bridge design AS 5100.2 Part 2: Design loads AS 5100.4 Part 4: Bearings and deck joints AS 5100.6 Part 6: Steel and composite construction NZS 1170.5 Structural Design Actions - Part 5: Earthquake design actions - New Zealand NZS 3404 Parts 1 & 2: Steel Structures Standard AS/NZS ISO 9001 Quality management systems – Requirements

ASTM International ASTM A276 Standard Specification for Stainless Steel Bars and Shapes ASTM A240M Standard specification for chromium and chromium-nickel stainless steel plate, sheet, and strip for pressure vessels and for general applications ASTM C794 Standard test method for adhesion-in-peel of elastomeric joint sealants ASTM D217 Standard Test Methods for Cone Penetration of Lubricating Grease ASTM D972 Standard test method for evaporation loss of lubricating greases and oils

International Standards EN 1337 Structural bearings EN 1337-2 Part 2: Sliding elements EN 1337-5 Part 5: Pot bearings EN 12163 Copper and copper alloys. Rod for general purposes EN 12164 Copper and copper alloys. Rod for free machining purposes EN 1337 Structural bearings ISO 752 Zinc ingots ISO 3274 Geometrical Product Specifications (GPS) – Surface texture: Profile method – Nominal characteristics of contact (stylus) instruments ISO 13000-1 Plastics – Polytetrafluoroethylene (PTFE) semi-finished products Part 1: Requirements and designation

Austroads ATS 5410 Steel Fabrication ATS 5420 Supply of Bolts, Nuts and Washers ATS 5610 Compression Seal Expansion Joints ATS 5570 Installation of Bearings

Waka Kotahi NZ Transport Agency SP/M/022 Bridge Manual

Australian Paint Approval Scheme APAS 2911 Polyurethane coating for protection of steel APAS 2972 Low build epoxy two-pack coating for the long term protection of steel in atmosphere

Department of Transport Victoria BTN 24 Code of Practice Bearings - AS 5100 Part 4

Transport for NSW BTD 2018/01 Bridge Bearings

Queensland Department of Transport and Main Roads Design Criteria for Bridges and Other Structures MRTS81 Bridge Bearings

# Definitions

In addition to the following definitions, the definitions and abbreviations in AS 5100.4 apply to this Specification:

| Bearing internal surfaces: | The internal surfaces of the pot, the face of the piston in contact with the elastomeric disc, the rim of the piston and the areas covered by the stainless steel plates and the sliding pads and strips. |
| --- | --- |
| Bearing group: | Bearings of the same type, with the same pot and piston geometry and with similar load capacity, for the purpose of testing. Bearings within a group may have different translational movement ranges. |
| Elastomer: | A macromolecular material that rapidly regains its approximate original dimensions after release of a weak stress that has caused its substantial deformation. |
| Elastomeric disc: | A disc of rubber fitted with internal seals around its perimeter that allows relative rotation of the top and bottom parts of the bearing |
| External seal: | The component used to seal the gap between the piston and the pot. |
| Internal seal: | The sealing ring(s) recessed into the face of the elastomeric disc and being in contact with the piston that prevents the disc from extruding from the pot. |
| Principal’s Registration Scheme: | Any scheme for the prequalification, registration or approval of products, manufacturers, suppliers and/or Professional Engineers in operation in the jurisdiction where the concrete is to be placed. |
| Sliding plate: | A steel plate in a sliding bearing fitted with a sliding surface to allow relative movement between the plate and the bearing. |
| Stainless steel bearing: | A pot bearing with its main steel components manufactured from stainless steel. |
| Structural steel bearing: | A pot bearing with its main steel components manufactured from structural (carbon) steel, except for the stainless steel sliding surfaces. |
| Professional Engineer: | A person who: - is registered on any scheme of registration of engineers prescribed by legislation in the applicable jurisdiction; - is appropriately registered or prequalified, if the Principal has implemented an applicable registration or prequalification scheme; and - satisfies at least one of the following requirements: is a Chartered Professional Engineer; or holds a 4-year civil engineering degree from a university that is accredited under the Washington Accord and is registered in a relevant area of practice on the National Engineering Register (in Australia) or the Register of Chartered Professional Engineers (in New Zealand). |
| Surface roughness parameter (Ra): | Measurement of roughness of a surface as specified in ISO 3274. |

# Quality System Requirements

The Contractor must prepare and implement a Quality Plan that includes the documentation in Table 4.1.

Table 4.1 Quality Plan

| Clause | Description of Document |
| --- | --- |
| 4.2 | Evidence of AS/NZS ISO 9001 certification |
| 5.8 | Design Documentation and Certification |
| 7.24 | Procedure for welding of stainless steel sheet |
| 7.32 | Procedure for bonding and lubricating the PTFE pad. |
| 8 or 9 | Procedure for protective treatment. |
| 10 | Procedure for dismantling and reassembly of test bearings. |

| HOLD POINT 1. |  |
| --- | --- |
| Process Held | Fabrication of bearings. |
| Submission Details | The Quality Plan must be provided at least 15 working days prior to the supply of the bearings. |

The manufacturer / supplier of the bearings must have a quality management system in place which is certified as compliant AS/NZS ISO 9001, by an organisation accredited by JAS-ANZ or an affiliated international certification organisation.

Where a Principal’s Registration Scheme is in place for the supply of bearings, the bearings must be approved under that scheme.

# Design

## General

Bearings must be designed in accordance with:

- the additional design requirements in the document listed in Table 5.1 (where applicable to the jurisdiction where the bearing is being installed);

- AS 5100.4; and

- EN 1337 and relevant European Technical Approvals.

- The above order of precedence applies in the event of an inconsistency.

Table 5.1 Additional Design Requirements

| Jurisdiction where the bearing is to be installed | Additional Design Requirements |
| --- | --- |
| Queensland | Design Criteria for Bridges and Other Structures. MRTS 81. |
| New South Wales | BTD 2018/01. Bearings must be approved by Transport for New South Wales. Refer to https://roads-waterways.transport.nsw.gov.au/business-industry/partners-suppliers/documents/tenders-contracts/listofapprovedbridgecomponentssystems.pdf |
| Victoria and Tasmania | BTN 24. |
| New Zealand | The bearings must be designed to the limit states applicable to seismic resistance in accordance with NZS 1170.5 and SP/M/022. |

Bolts must be designed in accordance with AS/NZS 5100.6. For bearings installed in New Zealand, NZS 3404 may be used as an alternative to AS/NZS 5100.6 for design of the bolts.

Steel components must be designed in accordance with to AS/NZS 5100.6. The relevant capacity reduction factors must not be less than those specified in AS/NZS 5100.6, even if the Principal approves an alternative design standard.

Bearings must be designed for Serviceability Limit Sate (SLS) and Ultimate Limit State (ULS) effects.

All associated sliding surfaces must be designed to accommodate the ULS movements plus an additional movement of ± 25 mm.

The guide bars must be designed to withstand the lateral forces shown on the Drawings and dimensioned such that the bearing movement remain guided throughout the specified limits of translation and rotation.

The design of the bearing must:

- allow for construction tolerances in the design and fabrication of the bearings and attachment plates, where required for the construction method adopted;

- enable the fasteners connecting the bearings to the attachment plates can be replaced without lifting the bridge superstructure;

- allow their removal at a maximum jacking lift of 10 mm (unless specified otherwise on the Drawings);

- ensure that the bearing attachment plates, and anchor bolts do not obstruct the movement and rotation of the bearing and allow its removal and replacement.; and

- provide for mechanical lifting and handling of the bearings where required.

## Design Documentation and Certification

The Quality Plan must include the following documentation for each bearing group:

- confirmation of all load cases (axial and shear loads, and rotation and movement in each direction, as applicable);

drawings of the assembled bearing and attachment plates to scale providing sufficient dimensions to enable design checking of components, including elastomer pad thickness;

design calculations of the bearing including mean compressive stress on the elastomer, sliding pad mean and peak pressures, maximum bearing stress on substructure and superstructure giving method of calculation, forces on bolts and dowels with required sizes and grades, and stress checks on steel structural components;

- where an approved bearing is proposed, any variations from the details of the bridge proprietary bearing as approved by the road agency; and

a certificate from a Professional Engineer, with at least 5 years of experience in structural engineering which is relevant to bridge bearings, verifying that all bearings and attachments comply with the requirements of the Drawings and this Specification.

# Materials

## General

Testing must be carried out at laboratories meeting the requirements specified in Clause 10.1.

## Ferrous Materials

Ferrous Materials must comply with Table 6.2.

Table 6.2: Ferrous Materials

| Application | Requirement |
| --- | --- |
| Pot, Piston, Sliding Plate, Guide Bars and Attachment Plates for Structural Steel Bearings | Structural steel conforming to AS/NZS 3678 and/or AS/NZS 3679.1 or approved equivalent. |
| For welded components | Austenitic stainless steel conforming to ASTM A240M (1) Grade 316 L (2) or approved equivalent |
| For components not to be welded | Austenitic stainless steel conforming to ASTM A240M (1) Grade 316 L (2) / Grade 316 (2) or approved equivalent. |
| Structural steel attachment plates (e.g., top attachment plate to steel girders) | Structural steel conforming to AS/NZS 3678 and/or AS/NZS 3679.1 or approved equivalent. |
| Sliding surfaces made from stainless steel sheets | ASTM A240M Grade 316 L or equivalent. The minimum thickness of stainless steel sheets is 1.5 mm for sheets with their larger dimension being less than 800 mm, and 2.5 mm for larger sheets. The sliding surface of the stainless steel sheet must be 2B surface finish, mechanically polished to mirror finish with the surface roughness not rougher than Ra of 0.4 µm. |
| Bolts, nuts, screws and washers | Compliance with ATS 5420 |
| Stainless steel dowels | ASTM A276 Grade 316L or equivalent for welded components. Grade 316 otherwise. |

Notes:

(1) 	Rolled plates must be used in fabrication, per the referenced standard. The Principal must be notified immediately, and directions sought if suitable rolled plate sizes cannot be sourced.

(2) 	Stainless steel Grade 316 /Grade 316L may not provide adequate corrosion protection for the exposed surfaces of bearings located at high chloride environments. In such cases, the details of a more superior material grade or/and additional surface protection must be submitted to the Principal for approval.

## Sliding Pads and Strips

Polytetrafluoroethylene (PTFE) sheets for sliding pads and guide sliding strips must be made from 100% virgin PTFE conforming to ISO 13000-1 Grade 1 and etched on the side which is bonded to the steel.

The minimum thickness of PTFE is 4.5 mm for sliding pads or guide sliding strips with no dimension exceeding 650 mm, or 6 mm for pads or strips with larger dimensions.

Sliding pads must be made from unfilled PTFE dimensionally stabilised moulded sheet and must be dimpled and lubricated in accordance with AS 5100.4 on the face in contact with the sliding surface.

Guide sliding strips must be:

- made from durable filled PTFE, with the fillers being either milled glass fibre (25% maximum) or carbon fibre (25% maximum); or

- a multilayered composite material, e.g., a three layer composite comprising a bronze backing strip, a sintered interlocking porous impregnated matrix, and an overlay of PTFE/lead, graphite/lead or similar mixture.

Guide sliding strips do not need to be dimpled.

## Elastomeric Disc

The elastomer used in the elastomeric disc must be 100% virgin natural rubber (polyisoprene). The elastomer must be plain, not laminated or fibre reinforced, and cured to satisfy the properties specified in Appendix B of AS 5100.4 for Type 50H.

## Internal Seals

Internal seals must be made of polyoxymethylene (POM), or carbon filled PTFE complying with EN 1337-5 or equivalent. Evidence demonstrating faultless field performance of the seal type proposed must be provided.

Alternatively, internal seals may be made from rectangular brass sections conforming to AS/NZS 1567 (half-hard). Where the zinc content in the brass is greater than 15%, the brass must be inhibited against dezincification. Brass seals made of grade CuZn37 to EN 12163 or grade CuZn39Pb3 to EN 12164 are acceptable.

## Lubricant

Lubricant for filling the dimples in the PTFE sliding pad and lubricating elastomeric disc must be made of silicone compounds. The lubricant must comply with Table 6.11.

Table 6.11: Properties of Lubricant

| Property | Method of Test | Requirements |
| --- | --- | --- |
| Worked penetration | ASTM D217 | < 260 (1, 2) |
| Evaporation after 22 hr at 150°C | ASTM D972 | < 2% |

Notes:

- Unit of measurement is one tenth of a millimetre.

- Penetration results up to 295 may be accepted for lubricants complying with the requirements of EN 1337-2 and EN 1337-5.

The lubricant must retain its room temperature consistency over a temperature range of – 40°C to + 200°C and be compatible with all the components in contact with it.

## Material Conformity

Documentary evidence, including certificates of compliance, to verify that all materials conform to the requirements of this Specification, must be provided to the Principal:

Testing must be carried out at laboratories as specified in Clause 10.1.

# Fabrication

## General

The bearings must comply with AS 5100.4 (in Australia) or SP/M/022 (in New Zealand) as amended by this Specification.

All fabricated items of the bearings must be free from defects including weld spatter.

All sharp edges, corners and weld crests must be rounded to a minimum radius of 1.5 mm and the edges of drilled holes chamfered.

## Flatness of Surfaces

The flatness along the profile of the following surfaces must not exceed the tolerance specified in Table 7.4.

Table 7.4: Flatness

| Surface | Maximum deviation from the specified surface profile |
| --- | --- |
| Bearing internal surfaces | 0.005 times the nominal dimension. |
| Plane sliding surfaces | 0.0003 times the larger dimension of the sliding material or 0.2 mm, whichever is greater. |
| Contact surfaces of pots, any intermediate plates, tapered or otherwise, and attachment plates where they are in contact with each other | 0.0003 times the nominal dimension or 0.2 mm, whichever is greater. |
| Contact surfaces of pistons, any intermediate plates, tapered or otherwise, and attachment plates where they are in contact with each other | 0.0003 times the nominal dimension or 0.2 mm, whichever is greater. |
| Contact surfaces of guide bars | 0.001 times the nominal dimension |
| Attachment plate surfaces other than those in contact with bearing top and bottom plates | Conform to the requirements of Specification ATS 5410. |

## Pot

The pot internal diameter must not exceed the piston rim diameter by more than 1.0 mm for bearings with metallic or POM internal seals, or 0.8 mm for bearings with PTFE seals.

The internal surfaces of the bearing must comply to the flatness specified in Clause 7.4 and to a maximum surface roughness Ra of 6.3 µm.

The cylinder and base plate of the pot must be fabricated from a single piece of steel complying with Clause 6.2. However, welding of a separate base plate to the cylinder may be approved if supporting design calculations and/or experimental evidence are submitted to the Principal showing that the strength of the welded component is equivalent to that made from a single piece of steel. Any welding must be Category SP or better conforming to the relevant part of AS/NZS 1554.

For bearings which will be subjected to uplift loading at ULS, inspection of the welding (if any) of ancillary elements of the bearings designed to carry the uplift loading must be carried out as follows:

- magnetic particle (for carbon steel) or liquid penetrant (for stainless steel) on 100% of the weld; and

- ultrasonic testing on at least 20% of the weld of each element, unless directed otherwise by the Principal.

## Piston

The piston must be machined from a single piece of steel complying with Clause 6.1.

If the thickness of the contact rim exceeds 15 mm or the bearing ULS rotation exceeds 0.025 radians, the contact rim face of the piston that bears against the pot wall must be bevelled or curved.

## External Seal

The gap between the pot and the piston must be sealed against dust and moisture using either a small compression seal with material properties that conform to ATS 5610 or a neutral cure silicone sealant or approved equivalent.

The seal must be able to accommodate the maximum ULS movements without being damaged.

## Elastomeric Disc

Each elastomeric disc must be manufactured from an individually moulded rubber slab and lubricated with a lubricant complying with Clause 6.11.

In the unloaded condition, the lateral clearance between the pot and the elastomeric disc must not exceed 0.2% of the diameter of the elastomeric disc or 0.5 mm, whichever is greater.

## Internal Seal - POM or Carbon Filled PTFE

POM seal rings, where applicable, must be made from individual interlocking elements and moulded as an integral part of the elastomeric disc during the vulcanisation process.

Carbon filled PTFE seal rings, where applicable, must be completely recessed into the elastomeric disc.

## Internal Seal - Brass

Brass seals must consist of a number of split rings formed to fit snugly in recesses in the elastomeric disc and within the inside wall surface of the pot. Each ring must contain one vertical cut, made at 45° to the tangent, with a maximum gap of 1 mm.  Install the rings such that the cuts of the individual rings are staggered equally or by a minimum of 90° relative to one another when the rings are fitted to the elastomeric disc.

The minimum number of rings must be two. Three rings must be used where the outside diameter of the ring is greater than 700 mm or the specified rotational capacity is greater than 0.025 radians.

The minimum thickness of each ring is 1.5 mm. The minimum width of rings must be 6 mm for ring diameters not exceeding 300 mm, and 10 mm for rings with larger diameters.

The maximum surface roughness Ra of the rings is 6.3 µm.

## Stainless Steel Sliding Surface

The stainless steel sheet in the assembled bearing must be larger than the PTFE pad, extending beyond the edges of the PTFE pad to accommodate the limits of translation specified in Clause  5.5.

The stainless steel sheet must be attached to the backing plate by continuous welds along the edges. The backing plate must extend beyond the stainless steel sheet to accommodate the welds.  The welded perimeter of the stainless steel sheet must not come in contact with the PTFE.

Welding must conform to AS/NZS 1554.6 Category 2B, surface condition II. Prequalified welding consumables must be used in accordance with AS/NZS 1554.6 for the combination of materials involved. The weld size must not exceed the thickness of the stainless steel sheet.

The Quality Plan must include welding procedures in accordance with AS/NZS 1554.6. The welding procedures must detail the welding sequence necessary to eliminate distortion and to ensure flatness of the sheet and its full contact with the backing plate.

After welding, the flatness of the sliding sheet must conform to the requirements of Clause 7.4.

All welds and heat affected zones of the stainless steel sheet must be passivated and repolished to a maximum surface roughness Ra of 0.4 µm.

## Guide Bars

Each guide bar must be manufactured from one piece of steel. Where connected by screws, the guide bars must be recessed into the plane sliding plates, or the pistons or the pots, as applicable.

Alternatively, the guide bar and the connecting sliding plate may be manufactured from one piece of steel by machining or by continuous welding around the bar to form a single piece.

The two contact surfaces of the guide bar(s) must be parallel to each other, with a flatness conforming to that specified in Table 7.4.

The maximum gap between a guide and its corresponding sliding surface must not exceed 3 mm when the other side is in full contact.

For each pair of mating sliding surfaces, a combination of stainless steel strip/sheet welded as specified in Clause 7.22 to one surface, and a sliding strip in accordance with Clause 6.6 for the corresponding sliding surface must be used. The sliding strip must be restrained by adhesive bonding and recessing and/or mechanical fixing

## PTFE Sliding Pad and Strips

PTFE must be restrained by adhesive bonding and recessing it into the backing material to a depth conforming to AS 5100.4 to prevent its extrusion with the protrusion being not less than that specified in EN 1337-2.

The average adhesion-in-peel strength of the adhesive compound must not be less than 30 N when tested under standard conditions to ASTM C794.

The backing material to the PTFE and the mating surface must be flat and rigid so that the PTFE layer will be uniformly loaded. The flatness of non-metallic sliding surfaces must conform to the requirements of Table 7.4.

The shoulder of the recess into the backing material must be sharp and square to resist extrusion of the PTFE. There must not be any gap between the inner face of the recess and the PTFE.

The PTFE pad must be permanently lubricated in accordance with AS 5100.4.

## Attachment Plates

Separate structural steel attachment plates must be used above and below the bearings. The minimum mean thickness of the attachment plates is 20 mm.

Attachment plates may be tapered to correct lack of parallelism caused by various effects including longitudinal grade, crossfall in the carriageway and hog or camber of the superstructure.

# Protective Treatment – Structural Steel Bearings

## General

This Clause 8 only applies to Structural steel bearings.

All work required for the protective treatment must comply with the requirements of AS/NZS 2312.1 or AS/NZS 2312.2, as relevant, and this Specification.

The coating systems for the bearing and attachment plates must be in accordance with Table 8.3.

Table 8.3: Coating Systems for Bearings and Attachment Plates

| Component | System |
| --- | --- |
| Bearing External Surfaces | Hot dip galvanised and painted to achieve a minimum of 50 years life to first maintenance; or ZP (1) |
| Bearing Internal Surfaces which are fully shielded from environmental effects | No treatment (4) |
| Attachment Plates | HDG (2) or ZP (1) |
| Fasteners | HDG (2) |
| Stainless Steel Sheet | No treatment (3) |

Notes:

- ZP: Zinc metal spray and paint system as detailed in Annexure B.

- Hot Dip Galvanising: Refer to Clause 8.13.

- Do not coat stainless steel sliding surfaces and protect these surfaces from being coated or damaged during the application of the protective treatment to adjacent areas.

- A coating must not be applied to any Bearing Internal Surfaces. Primer may be applied to the recess for PTFE but do not apply any treatment below the stainless steel sheet on the backing plate to prevent interference with welding.

The protective treatment must be applied under factory conditions prior to assembly of the bearings. Any repairs to damaged coatings must be carried out in accordance with the paint manufacturer’s instructions.

The protective treatment of the attachment plates, where attached to steel girders, must be the same as that of the steel girders.

All paints must be from a single manufacturer and comply with APAS 2911or APAS 2972. Details of paint used must be recorded.

## Surface Preparation

Steelwork surfaces which are to receive protective treatment must be cleaned, except those to be galvanized, by abrasive blasting in accordance with AS 1627.4, using crushed sharp angular metallic abrasive grit.

Before abrasive blasting, the areas contaminated with oil, grease, fingerprints, salt residues or other contaminants must be cleaned using alkaline solutions in accordance with AS 1627.1.

Steelwork surfaces to be galvanized in accordance with AS/NZS 4680 and AS/NZS 1214 must be prepared as appropriate.

## Zinc Metal Spray

Zinc metal must be applied using an electric arc spray method for melting the zinc wire. The spray must be applied to dry, dust free and clean surfaces within 24 hours after abrasive blasting to avoid any discolouration or contamination of the surfaces.

The temperature of the steelwork must be at least 3°C above the dew point.

The specified coating thickness must be the minimum local thickness on the significant surface of a single component in the bearing. The zinc metal coating must be sealed with an appropriate sealer prior to application of the top coat.

## Hot-Dip Galvanizing

Hot-dip galvanizing must be carried out in accordance with AS/NZS 4680 for applicable attachment plates and AS/NZS 1214 for fasteners.

All galvanized items must be quenched in a passivating chromate solution immediately after galvanizing.

## Paint Application

Paint must be applied using airless or air-assisted airless spraying methods to zinc sprayed steelwork no later than 24 hours after the zinc spraying. A stripe coat of paint to all edges of the surfaces to be painted must be applied prior to spraying. Shadowed areas must be brushed before spraying.

paint coats must be applied under the environmental conditions specified by the paint manufacturer. Finished paintwork must be cured for a minimum of three days before dispatch of bearings to site, unless otherwise recommended by the manufacturer.

# Protective Treatment – Stainless Steel Bearings

## General

This Clause 9 only applies to Stainless steel bearings.

Unless approved otherwise, a protective treatment must not be applied to any stainless steel component.

Where attached to steel girders, the protective treatment of any structural steel attachment plates must be the same as that of the steel girders.

## Insulation

The stainless steel bearing must be insulated from the structural steel attachment plates (where used) using suitable flat sheets, bushes and washers of at least 3 mm thickness, at the interface between the pot bearing and the attachment plates and around the bolts to the attachment plates.

The flat sheets, bushes and washers must be made of resin laminated sheets and tubes made from an electrical insulating material complying with the performance requirements of Table 9.5 must be used.

Table 9.5: Performance Requirements for Insulating Material

| Property | Method of Test | Requirements |
| --- | --- | --- |
| Insulating resistance after immersion in water | BS EN 60893-2 | ≥ 5 x 1010 Ω |
| Water absorption (3 mm) |  | ≤ 50 mg |
| Impact strength, notched Charpy |  | ≥ 10 kJ/m2 |

Holes must be matched drilled through the insulating sheet to accommodate the fixing screws to the top attachment plate.

# Testing

## General

Unless approved otherwise by the Principal, testing must be performed by a laboratory which is accredited for the test by a body that is a signatory to the International Laboratory Accreditation Cooperation Mutual Recognition Arrangement (ILAC MRA). The National Association of Testing Authorities (NATA) and International Accreditation New Zealand (IANZ) are signatories to ILAC MRA.

Bearings must be tested in accordance with this Clause 10 at the frequency specified in Table 10.2. The vertical, lateral and rotation load tests must be carried out on the same bearing.

Table 10.2: Frequency of Testing

| Method of Test | Bearings per Group |  |  |
| --- | --- | --- | --- |
|  | ≤ 10 | > 10 and ≤ 25 | ≥ 25 |
| Geometrical verification | All |  |  |
| Vertical load test | 1 per group | 2 per group | 3 per group |
| Lateral load test |  |  |  |
| Rotation capacity test |  |  |  |
| Coefficient of friction test | 1 per stainless steel batch and PTFE batch combination (1) |  |  |

Note:

- The test results are only valid where the stainless steel batch and PTFE batch combination tested is the same as that used for the bearings represented by the test sample. Past test results not more than two years old obtained for previous projects for the same PTFE and stainless steel batches may be accepted by the Principal.

| WITNESS POINT 1. |  |
| --- | --- |
| Process | Testing of bearings |
| Notification | At least 7 days prior to the commencement of testing. |

Bearings must be tested fully assembled, but without the external seal.

Where bearings are required to resist uplift forces, they must be subjected to appropriate testing to confirm the adequacy of the design.

The direction of loads/rotations applied in all the tests must replicate the design conditions.

On completion of each load test, the bearing must be dismantled and inspected for the defects listed in Clause 10.19. All sliding surfaces and elastomeric discs must be re-lubricated and the external seal installed for final assembly.

## Geometrical Verification

Bearing dimensions, flatness, surface roughness and clearances must be checked to verify compliance with the requirements of Clauses 6 and 7.

Flatness in all directions must be measured using a precision straight edge sliding on the surface and feeler gauges.

## Load Tests

The types of load tests in specified in Table 10.9 must be carried out.

Table 10.9: Types of Load Tests Required

| Bearing Type | Vertical | Lateral | Friction | Rotation |
| --- | --- | --- | --- | --- |
| Fixed | Yes | Yes | No | Yes |
| Free sliding | Yes | No | Yes | Yes |
| Guided sliding | Yes | Yes | Yes | Yes |

The relevant load tests must be performed on the bearing nominated for testing.

## Vertical Load Test

Vertical load testing of bearings must be carried out using the following procedure:

- load the bearings in compression to the maximum ULS vertical load shown on the Drawings;

- maintain this load for one minute;

- release the load;

- reapply the load to the maximum ULS vertical load and maintain it for a minimum loading period of three minutes (the loading period is the time the bearing sustains a test load of at least 95% of the intended test load); and

- carry out a visual inspection of the bearing while under the second stage loading and report any sign of damage in accordance with Clause 10.19.

## Lateral Load Test

Bearings which are required to resist lateral forces must be tested by applying the following test loads:

- maximum ULS lateral load while loaded in compression to the concurrent minimum ULS vertical load shown on the Drawings;

- maximum ULS lateral load while loaded in compression to the concurrent maximum ULS vertical load shown on the Drawings.

In both cases, the vertical load must be applied first and then the lateral loads applied gradually. The test loads must be maintained for a minimum loading period of three minutes.

A visual inspection of the bearing while under the applied loading must be carried out and any sign of damage in accordance with Clause 10.19 reported.

## Rotation Test

The bearings must be loaded in compression to a test load of 0.7 times the maximum ULS vertical load shown on the Drawings while at the design rotation specified in the Drawings. This vertical load must be maintained for a minimum loading period of three minutes.

A visual inspection of the bearing while under the applied loading must be carried out and any sign of damage reported in accordance with Clause 10.19.

## Coefficient of Friction Test

Coefficient of friction testing of plane sliding surfaces of bearings must be carried out using the following procedure:

- apply vertical loads corresponding to vertical pressures on the PTFE pad of 5 MPa and 20 MPa, unless shown otherwise on the Drawings, at an ambient temperature between 5°C and 35°C.

- the test displacement must be equal to the design displacement value but not exceeding 50 mm.

- apply the vertical load and maintain it for three minutes before starting sliding.

- the test sliding speed must be in the range of 2.5 to 25 mm/minute.

- record the maximum horizontal force during sliding.

- repeat the sliding and the horizontal force measurements to obtain the average of five measurements.

- where bearings are tested in pairs, calculate the coefficient of friction of the bearings using the equation below:

Coefficient of friction = Average horizontal force / (2 x vertical load)

The measured coefficient of friction must not exceed the values specified in Table 10.18 for the relevant pressure on the PTFE.

Table 10.18: Coefficient of Friction for Lubricated Sliding Surfaces

| Property | PTFE pressure |  |  |  |
| --- | --- | --- | --- | --- |
|  | 5 MPa | 15 MPa | 20 MPa | ≥ 30 MPa |
| Maximum coefficient of friction (1) | 0.04 | 0.025 | 0.02 | 0.015 |

Note:

- Interpolate friction values linearly for intermediate PTFE pressures.

## Criteria for Acceptance

Any bearing that does not meet the requirements specified in this Clause 10 or exhibits any signs of damage during or after the testing must be rejected. These signs of damage include:

- splitting, extrusion or permanent deformation of the elastomer;

- tearing, cracking or permanent deformation of the PTFE sliding surfaces;

- cracking, indentation or permanent deformation of the internal seal or other part of the bearing;

- abrasive marks indicating abnormal contact between the metal surfaces of the bearing plates or piston and/or the pot; and

- failure or permanent deformations of guide bars.

If a bearing is rejected, test two additional bearings from the group of bearing represented by the failed bearing must be tested. If both bearings meet the requirements of this Specification, the Principal may accept the remaining bearings in the bearing group.  Should one or both of the bearings not meet the requirements of this Specification, each of the remaining bearings in the group must be tested for compliance.

## Test Report

A laboratory test report containing all details and the results of all load tests must be prepared and submitted to the Principal. The report must include:

- the load used for the vertical load test;

- the load used for the lateral load test;

- the vertical load and the rotation used for the rotation test;

- photographs of bearings during and at the end of each test;

- photographs of any visible failure; and

- any observations noted during the testing process.

## Bearing Report

A bearing report must be prepared and submitted to the Principal. The report must include:

- Certificate of Compliance, in accordance with Clause 6.13, that the materials comply with this specification;

- verification, in accordance with Clause 10.7, that the geometry of the bearing complies with this Specification;

- a summary of all test results with clear identification of the bearings tested; and

- verification and certification that all bearings conform to the requirements of this Specification.

# Identification and Delivery

Each bearing must be identified and fitted a nameplate to the bearing, including the applicable installation locations of the bearings.

The bearing orientation, the centreline and the direction(s) of movement as appropriate must be readily identifiable to facilitate correct placement.

| HOLD POINT 2. |  |
| --- | --- |
| Process Held | Delivery of bearings to site |
| Submission Details | The bearing test report in accordance with Clause 10 must be submitted at least 10 working days before the proposed date for delivery of bearings to site. |

Temporary transit clips or equivalent, which must be easily removable, must be provided to hold the bearing components assembled during delivery. The transit clips and/or bolts must not be removed until after completion of installation in the bridge structure unless approval is sought from and given by the Principal for operational reasons.

Bearings must be kept in dust and moisture resistant protective wrappings at all times prior to installation.

Mating parts of bearings must be supplied in sets held together at the correct preset and skew with metal transit clips and/or bolts to prevent misalignment and/or damage of the components during transport and erection.

The temporary constraints must be removed after installation to allow the bearings to function as intended.

Annexure A:	Summary of Hold Points, Witness Points and Records

The following is a summary of the Witness Points / Hold Points that apply to this Specification and the Records that the Contractor must submit to the Principal to demonstrate compliance with this Specification.

| Clause | Hold point | Witness point | Record |
| --- | --- | --- | --- |
| 4.1 | - Fabrication of bearings. |  | Quality Plan |
| 10.2 |  | - Testing of bearings |  |
| 10.21 |  |  | Test Report |
| 11.2 | - Delivery of bearings to site. |  | Bearing Report |

Annexure B:	ZP Coating System

### This Appendix B only applies if the ZP Coating System has been specified.

### B1	Coating System

The coating system consists of zinc coat, sealer and wet paint coating applied in their respective order.

### B2	Surface Preparation

- Abrasive blast cleaned to Class 3 in accordance with AS 1627.4.

- Nominal surface profile of 75 µm.

- Surface profile measured in accordance with Method A in AS 3894.5.

### B3	Zinc Coat

- Zinc wire: Zn 99.99 conforming to ISO 752.

- Minimum local thickness of 150 µm.

- Local coat thickness measured in accordance with AS 2331.1.3.

### B4	Sealer

- Sealer: a proprietary low viscosity sealer compatible with the top coat.

### B5	Wet Paint Coating Systems

- The wet paint coating systems must be either System A or System B in accordance with Table B5.

Table B5 – Wet Paint Coating Properties

| Description | System A | System B |
| --- | --- | --- |
| Paint | MIO epoxy | HB polyurethane |
| Description | A two pack micaceous iron oxide pigmented polyamide cured epoxy coating conforming to APAS 2972. | A full gloss two component, high build recoatable, acrylic modified polyurethane enamel, excluding two pack acrylic, included in a system conforming to APAS 2911. |
| Min DFT (µm) | 125 | 125 |
| Colour | Unless specified otherwise, colour ‘N44 Bridge Grey’ to AS 2700 | Colour N35 ‘Light Grey’ to AS 2700 |

Notes:

- System A applies unless specified otherwise.

Minimum DFT is the minimum dry film thickness measured in accordance with Magnetic Induction Method B in AS 3894.3.

Amendment Record

| Amendment no. | Clauses amended | Action | Date |
| --- | --- | --- | --- |
| - | New specification | New | March 2023 |

| Key |  |
| --- | --- |
| Format | Change in format |
| Substitution | Old clause removed and replaced with new clause |
| New | Insertion of new clause |
| Removed | Old clauses removed |