| # AUSTROADS TECHNICAL SPECIFICATION ATS 4450 Plastic Noise Walls |  |
| --- | --- |

Contents 1. Scope 1 2. Referenced Documents 2 3. Definitions 3 4. Quality System Requirements 4 5. Design 4 General 4 Design Life 5 Design Loads 5 Structural Design 6 Structural Robustness 6 Design for Inspection and Maintenance 6 Design Documentation 7 6. Acoustic Requirements 7 7. Constituent Materials 8 General Requirements 8 In-service Requirements 8 Transparent Panels 8 Testing of Panels 9 Fire Performance 10 Posts, Panel Fixings and Fasteners 10 8. Manufacture and Installation 11 General 11 Maintenance Manual 11 Warranty 11 Annexure A Summary of Hold Points, Witness Points and Records 12 Amendment Record 13

# Scope

Austroads Technical Specification ATS 4450 sets out the requirements for the design, manufacture and installation of noise walls using plastic panels, including those manufactured from recycled plastic. It excludes:

noise walls which are predominantly manufactured from materials other than plastic, such as aluminium, concrete, laminated safety glass, masonry, steel or wood;

panels attached to buildings; and

earth mounds created for noise attenuation purposes.

This Specification may also be used for the manufacture and installation of plastic panel walls erected for purposes other than noise attenuation (such as landscaping, fencing or aesthetics), in which case Clause 6 does not apply.

Unless specified otherwise in the Contract documents, this Specification does not apply to panels attached to bridge over a road, pedestrian path or other situation where there is a risk panels or fragments of panels from falling on to traffic or pedestrians as a result of vehicle impact.

# Referenced Documents

The following documents are referenced in this Specification:

Australian/New Zealand/ISO Standards ISO 717-1 Acoustics – Rating of sound insulation in buildings and of building elements – Part 1: Airborne sound insulation AS/NZS 1170 Structural design actions (series) AS 1191 Acoustics – Method for laboratory measurement of airborne sound transmission insulation of building elements AS 1530.8.1 Methods for fire tests on building materials, components and structures – Part 8.1 – Tests on elements of construction for buildings exposed to simulated bushfire attack – Radiant heat and small flaming sources AS/NZS 1580.601.1 Paints and related materials – Methods of test colour – Visual comparison AS/NZS 2208 Safety glazing materials in buildings AS 2312.2 Guide to the protection of structural steel against atmospheric corrosion by the use of protective coatings, Part 2: Hot dip galvanizing AS/NZS 3837 Method of test for heat and smoke release rates for materials and products using an oxygen consumption calorimeter AS/NZS 3845.1 Road safety barrier systems and devices, Part 1: Road safety barrier systems AS 4100 Steel structures AS/NZS 4680 Hot-dip galvanized (zinc) coatings on fabricated iron and steel articles – Specifications and test methods AS/NZS 4766 Rotationally moulded buried, partially buried and non-buried storage tanks for water and chemicals AS 5100 Bridge design Part 1 Scope and general principles Part 2 Design loads AS/NZS ISO 9001 Quality management systems ISO 10140-2 Acoustics – Laboratory measurement of sound insulation of building elements – Part 2: Measurement of airborne sound insulation AS ISO 11654 Acoustics – Rating of sound absorption – Materials and systems AS 14021 Environmental statements and programmes for products – Self-declared environmental claims AS ISO/IEC 17025 General requirements for the competence of testing and calibration laboratories

Austroads ATS-5335 Normal Class Concrete ATS-5850 Handling, Storage, Transportation and Erection of Structural Members

ASTM International ASTM D543 Standard Practices for Evaluating the Resistance of Plastics to Chemical Reagents ASTM D1746 Standard Test Method for Transparency of Plastic Sheeting ASTM D2565 Standard Practice for Xenon-Arc Exposure of Plastics Intended for Outdoor Applications ASTM D792 Standard Test Method for Density and Specific Gravity (Relative Density) of Plastics by Displacement ASTM E831 Standard Test Method for Linear Thermal Expansion of Solid Materials by Thermomechanical Analysis ASTM G21 Standard Practice for Determining Resistance of Synthetic Polymeric Materials to Fungi

Australian Building Codes Board NCC Vol 1 National Construction Code Volume 1

# Definitions

In following definitions apply to this Specification.

| Bushfire attack level (BAL): | A means of measuring the severity of a component or a structure’s potential exposure to ember attack, radiant heat and direct flame contact, using increments of radiant heat expressed in kilowatts per metre squared. For example, BAL 12.5 is based on an incident radiation of 12.5 kW/m2. |
| --- | --- |
| Design life: | The period adopted in design for which a structure or structural element is required to perform its intended purpose with periodic maintenance and without replacement or major structural repairs. |
| Manufacturer: | The entity responsible for the manufacture of the panel. |
| Principal’s Registration Scheme: | Any scheme for the prequalification, registration or approval of products, manufacturers and/or suppliers in operation in the jurisdiction where the noise wall is to be constructed. |
| Recycled plastic: | Waste plastic that has been collected and processed, by physical, chemical, or other means, and developed into a new product. |

# Quality System Requirements

The Contractor must prepare and implement a Quality Plan that includes the documentation listed in Table 4.1.

Table 4.1:	Quality Plan

| Clause | Description of document |
| --- | --- |
| 4.2 | Evidence of certification to AS/NZS ISO 9001 |
| 5.26 | Design documentation, including a Design Report and the Drawings |
| 6.1 | Acoustic Performance (only required if the wall is for the purpose of noise attenuation) |
| 7.1 | Details of the materials used in the panels |
| 7.8 | Test results of the materials used in the panels |
| 8.9 | Maintenance Manual |

| HOLD POINT 1 |  |
| --- | --- |
| Process Held | Commencement of installation of a noise wall |
| Submission Details | The Quality Plan must be provided to the Principal at least 10 working days prior to the commencement of the installation of plastic panels. |

The panels must be manufactured under a quality management system which is certified to AS/NZS ISO 9001 by a JAS-ANZ accredited organisation (or accredited by another Accreditation Body Member of the International Accreditation Forum).

Where a Principal’s Registration Scheme is in place for the supply of wall panels, the panels must be approved under that scheme.

# Design

## General

The wall must be designed in accordance with this Clause 5 and any additional requirements specified in the Contract documents, which may include:

an acoustic specification (not applicable if noise attenuation is not required);

the material type (reflective or absorptive); and

the wall location and dimensions.

- If these requirements are not included in the Contract documents, the Design Report must record these parameters and the decision making process used to determine them.

The wall must consist of posts and replaceable plastic panels. The panels must:

be inserted into rubber or similar gaskets which are located in metal channels;

have sufficient freedom to allow their normal range of thermal expansion and contraction without damage to the posts or panels while maintaining acoustic sealing of joints; and

be readily replaceable.

The design must consider the pattern of the sun movement and directional lighting (including car headlights), with panels being angled as appropriate. If necessary, a matte finish must be applied to prevent reflective glare from the sun or headlights being experienced by road users.

The walls may be freestanding or located on structures such as traffic barriers. Freestanding noise walls are installed on individual foundations in the form of bored piles or spread footings. The foundations must not impede natural drainage flow paths. Those installed on traffic barriers are typically located on bridges and bridge approaches.

The design of the posts supporting the panels must comply with AS 4100. If the noise wall is attached to a bridge or bridge approaches, the noise walls must also comply with AS 5100.1 and AS 5100.2.

Where a wall also performs as a road safety barrier system, it must also comply with the specified containment class as defined in AS/NZS 3845.1. If a free standing noise wall is protected by a traffic barrier, there must be sufficient clear distance between the traffic barrier and noise wall to account for traffic barrier deflection.

Where a wall interacts with other engineering structures (retaining walls, bridges, road safety barriers, etc.), design analysis of the supporting structures must account for the forces imposed by the wall on the structure.

Where a panel contains a central void, the panel must include a drainage hole, with a minimum diameter of 20 mm, to prevent any water pooling internally. The hole must be positioned at the base of the panel at the back, be out of sight and not impact the visual aesthetics of the panel.

## Design Life

Subject to Clause 5.5, the Design Life of the wall components must not be less than:

- Posts and other structural components:	50 years

- Panels, panel fixings and fasteners:	30 years.

## Design Loads

The wall, including the posts, must be designed for the loading determined in accordance with AS/NZS 1170. If the panel is attached to a bridge, the requirements of AS 5100.2 also apply, using the net design wind pressure for ultimate limit states and serviceability.

Regional wind speeds must be based on Table 3.1 of AS/NZS 1170.2 using the following average recurrence intervals (ARI):

- Ultimate – 1000 year ARI.

- Serviceability – 20 year ARI.

Where wall panels are vertically stacked, the underlying panels must not deform when exposed to a load of 1.35 times of the overlaying self-weight of the panels.

Panels must be designed with an allowable deflection of span /130 under the serviceability wind loading.

If the wall is located within 4.0 m of the edge line of a road which is zoned at 100 km/h or more, the design must include an additional serviceability loading of 0.65 kPa due to dynamic suction imposed by vehicles passing at highspeed.

The design must allow for the increased wind load near the ends of noise walls, according to Appendix D2 of AS/NZS 1170.2. Subject to achieving the required acoustic performance, the height of noise walls at the ends may be decreased to reduce wind loads and improve appearance.

## Structural Design

The design must take into account the effects of material degradation, warping, twisting, distortion and bowing, caused by any of the following:

- Temperature and temperature differentials;

- Moisture and moisture differentials; and

- The effects of an aggressive roadside environment, including UV radiation, vehicle exhaust fumes and graffiti removal,

Where the wall height is built up from vertically stacked panels, the load on panels must account for bowing of panels. The design must be based on the assumption that the panels will be stacked with bowing of adjacent panels such that the load distribution produces the worst load effects.

The bottom edge of the wall panel must be restrained against bowing and warping.

All structural support systems (including flexible edge seals) must be designed to effectively seal against noise and restrain the panels, accounting for the movements associated with warping, twisting and bowing.

Under the action of serviceability wind-loading only, the maximum horizontal deflection of a wall post must not exceed 0.67% of the post height.

## Structural Robustness

A wall must not become detached from its support or fixing, both in the horizontal and vertical planes, when subjected the ultimate wind load and the highest combination of the allowable tolerances on the manufacture of panels and installation of the wall.

The design of the panels must take the following into account:

- the creep deformation or rupture over the Design Life at the service conditions; and

- the panels must be sufficiently ductile to provide for deformation at the supports or alternatively flexible seals may be used.

## Design for Inspection and Maintenance

Unless specified otherwise in the Contract documents, to provide for inspection, maintenance, repair and emergency access, the noise wall must:

- be accessible from both sides; and

- if necessary, include openings to enable access for small maintenance machinery.

A free draining, near horizontal surface (minimum 1.0 m wide) must be constructed to both sides of any noise wall located on an earth mound or batter slope. The purpose of this surface is to:

- protect the foundation;

- ensure stability foundation of (sliding and overturning);

- prevent gap formation below the noise wall; and

- provide construction and maintenance access.

Noise walls, when placed on or in front of a structure, must not obstruct maintenance of the structure.

## Design Documentation

The design documentation (which includes a Design Report and the Drawings) must specify all requirements necessary to enable the wall to be manufactured and installed in accordance with this Specification. The Design Report must include design decisions, calculations and any other relevant information not included in the Drawings.

At a minimum, the Drawings must include details of:

the height, length and position of the wall;

the type of wall and panel material composition;

the method of fixing the panel;

the panel dimensions;

acoustic requirements (where applicable);

protective coatings;

the posts and foundations;

geotechnical information;

height and details of any structure that interact with the wall (in cross sections for each segment of the wall);

cadastral /road edge and property boundary;

existing and proposed infrastructure, drains, road safety barriers, signs, known utilities, fences and gates;

topographic data (existing and proposed) over the area of interest including the road;

drainage requirements; and

design wind speeds.

# Acoustic Requirements

This Clause 6 does not apply if the wall is not designed for noise attenuation.

The panels must be constructed of reflective and/or absorptive type material. Panels must have sufficient intrinsic airborne sound insulation performance to ensure that, for all receivers, the sound transmitted directly through the wall is ≥ 10 dB below the sound diffracted at the top of the wall. The following is deemed to satisfy this requirement:

- A construction that has a sound insulation rating value of the weighted sound reduction index with spectrum adaptation term Rw + Ctr of at least 25 dB determined in accordance with ISO 717-1.

The laboratory measurements of airborne sound insulation must be conducted in accordance with AS 1191 or ISO 10140-2, with the test specimen mounted and assembled as in its intended use (i.e. the correct side must face the loudspeaker(s) in the source). At least one post must be included in the test specimen, with panels attached on both sides, where posts are used in construction. The length of the panel on one side of the post must be ≥ 2 m.

In addition to the minimum Rw requirements in Clause 6.1, the following applies to absorptive noise walls:

- the Weighted Sound Absorption Coefficient of the noise wall panels must not be less than 0.8 (αw) measured in accordance with AS ISO 11654;

- the absorptive face must be on the traffic side; and

- absorption is not required in the noise wall between 0 mm and 500 mm above the ground.

The acoustic properties of the panel must be retested if a substantial change is made to the design of the panel, which includes a variation to the wall thickness and front face shape.

Unless specified otherwise, the design must include a reinforced concrete sill beam located directly under the underside of the lowest panel. The sill beam must be:

- detailed to maintain the integrity of the acoustic barrier and ensure that water does not pond in the vicinity of the wall;

- designed to prevent long term subsidence occurring; and

- constructed from N25 concrete (or a higher grade) in accordance with ATS 5335.

# Constituent Materials

## General Requirements

The Quality Plan must include the following:

- the composition of the materials, including constituents and the percentage by weight in the finished product, demonstrated by laboratory analysis;

- the proportion of recycled materials in the finished product (as defined in AS 14021);

- the source of the component materials;

- description of the process of recycling and combination of the materials (where applicable) including machinery, source, type and quantity of energy required by weight to produce the finished product; and

- test records demonstrating that the materials comply with Table 7.10.

## In-service Requirements

For the duration of the Design Life under service conditions, all materials must be stable when exposed to UV radiation, vehicle exhaust fumes and graffiti removal. All plastics must contain UV inhibitor.

Noise wall materials must be resistant to impact damage caused by vandalism.

Graffiti must be readily removable with the application of soap and high-pressure water.

Panels must be resistant to scratching and discolouration with age.

## Transparent Panels

Transparent panels must:

- be made from acrylic (PMMA) or PC (polycarbonate) unless details of the material are included in the Quality Plan and its use has been approved by the Principal;

- be classified as Grade A safety glazing material to AS/NZS 2208; and

- be tinted and patterned with thin opaque stripes (or similar) to avoid bird strikes.

During the Design Life of a transparent panel, mottling must not occur and a Colour Rating must be less than 2 according to AS/NZS 1580.601.1, taking into account the effect of an aggressive environment, including UV radiation, vehicle exhaust fumes and graffiti removal.

## Testing of Panels

Unless specified otherwise, all testing, calibration and/or sampling carried out to verify conformance with this Specification must be performed by a laboratory that is accredited to meet the requirements of AS ISO/IEC 17025 for the applicable test method. The laboratory’s accreditation body must be a signatory to the Global Accreditation Cooperation Incorporated (Global ACI) Multilateral Recognition Arrangement (MRA) for testing laboratories. The National Association of Testing Authorities (NATA) and International Accreditation New Zealand (IANZ) are signatories to the Global ACI MRA.

When submitted to the Principal, test certificates must not be older than 60 months for the accelerated exposure tests and 36 months for other tests.

The materials used in the manufacture of the noise wall must be tested for conformance with the requirements in Table 7.10. The testing must be repeated in the event of a change to the constituent raw materials, design or colour of the panels.

Table 7.10:	Materials properties

| Property | Test method | Acceptance criteria(1) |
| --- | --- | --- |
| Resistance to fire | AS 1530.8.1 | Refer to Clause 7.12 |
| Smoke release rate | AS/NZS 3837 | The smoke growth rate is ≤ 100(2) |
| Density | ASTM D792 | As specified by the designer |
| Strength and elastic modulus | As specified by the designer | As specified by the designer |
| Transparency | ASTM D1746 | As specified by the designer |
| Translucence | ASTM D1746 | As specified by the designer |
| Resistance to ultraviolet-light exposure (‘QUV Exposure’) | ASTM D2565 | No delamination, fading, discoloration, chalking, or embrittlement after 1,500 hours of exposure(3) |
| Impact resistance | AS/NZS 4766 Appendix C Low temperature impact | Resist an impact energy of 90 J at -40°C |
| Thermal expansion | ASTM E831 | The average expansion of the panel material is below the nominal design maximum (refer to Clause 5.2) for the material when exposed to weather conditions appropriate for location of noise wall |
| Resistance to vermin and micro-organisms | ASTM G21 | No growth of fungus observed |
| Resistance to chemicals, including oils and acids | ASTM D543 | No reported changes to panels in weight, dimensions, appearance, colour, strength, and other mechanical properties under exposure to methylated spirits, thinners and brake fluid |

Notes:

The properties specified in Table 7.10 may not be suitable for high risk applications, in which case additional requirements will be specified in the Contract documents.

Complies with NCC Vol 1, criteria for unsprinklered wall lining materials.

If only the material colour is changed, this test must be repeated, but the exposure period may be reduced to 500 hours.

## Fire Performance

The wall materials must achieve the requirements specified in Table 7.11.

Table 7.11:	Fire performance

| Cause of fire | Requirement |
| --- | --- |
| Small arson ignition | The fire does not spread beyond the immediate area of ignition. |
| Vehicle fire | The fire does not spread to the panel adjacent to the point of ignition. |
| Bushfire | The fire propagation along the wall is minimised when subject to BAL 12.5 (unless a higher BAL is specified in the Contract documents). |

Panels must be tested for resistance to fire in accordance with AS 1530.8.1, with modifications as follows:

- For panels larger than 1.0 m × 1.0 m, a test specimen with minimum dimensions of 
1.0 m × 1.0 m must be used.

- For panels with any dimensions smaller than 1.0 m, a test specimen of the largest dimensions available must be used.

- The test specimen must be supported in a vertical configuration.

- Crib type Class A must be used.

- The crib must be placed adjacent to and touching the test specimen.

- Flames must not spread to the extent of the tested specimen.

A burning panel must not emit harmful smoke or poisonous gas in a concentration which may be environmentally dangerous or exceed limits prescribed in any applicable legislation for management of the environment.

## Posts, Panel Fixings and Fasteners

All steel components must be hot-dipped galvanized in accordance with AS/NZS 4680 with a minimum average coating mass of:

- 600 g/m2 if located in a Medium (or less severe) Corrosivity Category;

- 900 g/m2 if located in a High (or more severe) Corrosivity Category,

- where Corrosivity Category is defined in AS 2312.2.

Refer to the Contract documents for any additional requirements for the materials used in the posts, panel fixings and fasteners.

# Manufacture and Installation

## General

The wall must be manufactured and installed in accordance with the Drawings and this Specification.

Each panel must have clearly embossed markings in a location that can be easily accessed and inspected, with the following information;

the Manufacturer’s name, contact details and address;

month and year of manufacture;

clear identification the topside; and

the Plastics Identification Code identifying the type of plastic used in the panels.

| WITNESS POINT 1 |  |
| --- | --- |
| Process | Installation of noise walls |
| Notification Period | At least 2 working days before the commencement of work on Site. |

Walls must be free of holes or gaps. This includes a gap between a panel and the earthworks or pavement material immediately below the panel.

Any drainage holes in a panel (refer to Clause 5.8) must be free from obstructions and be free draining.

Panels must not be drilled for mounting purposes. Self-tapping screws must not be used.

Prior to any site modification of a panel, the approval of the designer must be obtained and a copy of that approval submitted to the Principal. Hold Point 1 will then apply again.

The handling, storage, transportation and erection of the panels and other components must be carried out in accordance with ATS 5850.

Panels must be free of attachments (such as signs, brackets or advertising) of any kind.

## Maintenance Manual

The Quality Plan must include a Maintenance Manual which specifies the maintenance requirements and procedures for the wall, including:

procedure for removing graffiti;

recommendations for painting or other maintenance measures;

procedure for replacement in the event of fire damage a panel; and

procedures for repair or replacement in the event of other damage to a panel.

## Warranty

The panels must be supplied with a Manufacturer’s warranty in the name of the Principal. The warranty must:

cover defective design, material and manufacturing; and

continue for a minimum period of 5 years.

Summary of Hold Points, Witness Points and Records

The following is a summary of the Witness Points /Hold Points that apply to this Specification and the Records that the Contractor must submit to the Principal to demonstrate compliance with this Specification.

| CLAUSE | HOLD POINT | WITNESS POINT | RECORD |
| --- | --- | --- | --- |
| 4.1 | Installation of a noise wall |  | Quality Plan |
| 8.2 |  | Installation of noise walls |  |
| 8.10 |  |  | Warranty |

Amendment Record

| Edition no. | Clauses amended | Action | Date |
| --- | --- | --- | --- |
| 1.0 | New specification | New | May 2023 |
| 1.1 | 7.8 – Updated laboratory accreditation requirements. | Substitution | October 2026 |

| Key |  |
| --- | --- |
| Format | Change in format |
| Substitution | Old clause removed and replaced with new clause |
| New | Insertion of new clause |
| Removed | Old clauses removed |