| # AUSTROADS TECHNICAL SPECIFICATION ATS 5452 Hot Dip Galvanizing |  |
| --- | --- |

Contents 1. Scope 1 2. Referenced Documents 2 3. Definitions 2 4. Quality System Requirements 2 5. General 3 6. Pre-Galvanizing 3 7. Post-Galvaniing Requirements 4 8. Preparation of Galvanized Articles for Painting 4 9. Repair of Damaged Galvanized Coatings 5 10. Completion 5 Annexure A Summary of Hold Points, Witness Points and Records 6 Amendment Record 7

# Scope

Austroads Technical Specification ATS 5452 sets out the requirements for the hot dip galvanizing of steel articles where the galvanized coating is applied after fabrication. This includes the coating of fabricated structural steel sections, fabricated steel assemblies, castings and miscellaneous steel components.

ATS 5452 does not cover:

the galvanizing of threaded fasteners; and

the galvanized coating produced in continuous, semi-continuous or specialised plants on semi-finished products, such as wire, strip, tube, sheet or coil.

The Contractor must ensure that the Galvanizer complies with this Specification.

# Referenced Documents

The following documents are referenced in this Specification:

Australian/New Zealand Standards AS 1627.1 Metal finishing – Preparation and pretreatment of surfaces, Part 1: Removal of oil, grease and related contamination AS 1627.4 Metal finishing – Preparation and pretreatment of surfaces, Part 4: Abrasive blast cleaning of steel AS/NZS 2312.2 Guide to the protection of structural steel against atmospheric corrosion by the use of protective coatings, Part 2: Hot dip galvanizing AS/NZS 3750.9 Paints for steel structures, Part 9: Organic zinc-rich primer AS/NZS 3750.15 Paints for steel structures, Part 15: Inorganic zinc silicate paint AS/NZS 4680 Hot dip galvanized coatings on fabricated iron and steel articles – Specifications and test methods AS/NZS 5131 Structural steelwork – Fabrication and erection AS/NZS ISO 9001 Quality management systems – Requirements

Australian Paint Approval Scheme (APAS) AP-S0014 Zinc Rich Pre-construction Primers (sub-class 0014/2) AP-S2916 Organic Zinc-Rich Coating for the Long-Term Protection of Steel (sub class 2916/1) AP-S2908 Inorganic Zinc Silicate Coating for the Long-Term Protection of Steel

ASTM International ASTM B201 Standard Practice for Testing Chromate Coatings on Zinc and Cadmium Surfaces

# Definitions

The definitions in AS/NZS 4680 and AS/NZS 2312.2 apply to this Specification.

# Quality System Requirements

The Contractor must prepare and implement a Quality Plan that includes the documentation in Table 4.1.

Table 4.1:	Quality Plan

| Clause | Description of document |
| --- | --- |
| 5.1 | Name of the Galvanizer and general galvanizing requirements. |
| 5.4 | Name, qualifications and experience of the Coating Inspector. |
| 6.1 | Procedures/details for pre-galvanizing. |
| 7.1 | Procedures/details for post-galvanizing. |
| 8.2 | Details and other requirements where a duplex coating is applied. |
| 9.1 | Procedure for repair of damaged or uncoated areas. |

| HOLD POINT 1 |  |
| --- | --- |
| Process Held | Commencement of galvanizing. |
| Submission Details | The Quality Plan must be provided to the Principal at least 10 working days prior to the commencement of galvanizing. |

# General

The Quality Plan must include:

- name of the Galvanizer and details of the galvanizing facilities;

- details of the hot dip galvanizing bath size, article size and any requirement for double dipping of the article; and

- whether any ultra-low reactive steels, in accordance with Clause 4.5.1 of AS/NZS 4680, will be used.

The design of the article must comply with AS/NZS 2312.2.

The galvanizing must comply with this Specification and all recommended requirements in AS/NZS 4680.

Unless the Contract documents specify that the Principal will appoint the Coating Inspector, the Contractor must ensure that a Coating Inspector is engaged to independently verify that the galvanizing complies with this Specification. The Coating Inspector must hold a current accreditation which is acceptable to the Principal. The ACA/GAA Hot Dip Galvanizing Inspector Program is acceptable to the Principal.

The Coating Inspector must independently and impartially monitor the Galvanizer’s activities to verify that the Galvanizer has complied with this Specification.

The Contractor must provide at least 48 hours of notice prior to the commencement of galvanizing.

| WITNESS POINT 1 |  |
| --- | --- |
| Process | Commencement of galvanizing of the articles. |
| Notification Period | At least 48 hours before the commencement of the work. |

# Pre-Galvanizing

The Quality Plan must include:

- a procedure for undertaking the inspection of the article prior to the galvanizing process and managing any corrective action necessary;

- details of the location of where the inspection will be conducted; and

- an Inspection and Test Plan for the inspection of the article prior to the galvanizing process.

Prior to the commencement of galvanizing, the Galvaniser must verify that:

the article complies with all clauses in AS/NZS 5131 that are relevant to galvanising;

the surfaces comply with AS/NZS 5131, Clause 9.8.4, Treatment Grade P3; and

the size and location of vent and drain holes comply with the requirements of AS/NZS 2312.2.

After fabrication and before the galvanizing process commences, the article must be inspected by the Coating Inspector to verify that the article complies with this Clause 6.

# Post-Galvaniing Requirements

The Quality Plan must include:

a procedure for carrying out the inspection for conformance to AS/NZS 4680;

an Inspection and Test Plan to verify conformance to AS/NZS 4680, including:

the appearance conforms to Clause 4.1 of AS/NZS 4680;

the thickness of the galvanizing conforms to Clause 4.2 of AS/NZS 4680; and

procedures to minimise wet storage staining and prevent handling damage after completion of the hot dip galvanizing process.

At the completion of galvanizing, the Coating Inspector must carry out inspection and testing in accordance with the requirements of AS/NZS 4680.

In addition to the requirements of AS/NZS 4680, galvanized coatings must also be free from defects that may affect the long-term performance of the coating, including brittle, uneven and/or loosely adhering coatings.

Further to Clause 4.1 of AS/NZS 4680, touch points from hanging wires, chains or jigs are acceptable, provided that they are not sharp and the galvanizing meets the thickness requirements.

The galvanized coating thickness must meet the requirements of AS/NZS 4680 Table 3, Table 4, or Table 5 as appropriate. Non-destructive test methods that are consistent with AS/NZS 4680 must be used to determine the coating thickness.

A test report, as described in AS/NZS 4680 Section 5, must be prepared by the Coating Inspector and submitted to the Principal (refer to Clause 10).

Any crevices or gaps between steel surfaces present after galvanising must be sealed using a two-part solvent-less epoxy putty or suitable sealant that has been approved by the Galvaniser.

# Preparation of Galvanized Articles for Painting

This Clause 8 applies where a duplex system will be applied to the article.

The Quality Plan must include:

details of the proposed surface finish;

details of any specific after-treatment requirements, including verifying that the article will be suitable for sweep or brush blast cleaning as described in AS/NZS 2312.2;

if a passivation treatment is used to protect freshly galvanized surfaces from early wet storage staining, details of that treatment; and

if it is proposed to exclude a passivation treatment, the maximum time between galvanizing and painting, any additional surface preparation steps and a description of the risk of wet storage staining or other defect occurring prior to painting.

The galvanized surface must be prepared in accordance with Clause 7.5.3 of AS/NZS 2312.2 so that the surface is free of salts, loose particles, paint overspray, dust or any other surface contaminants.

The lead acetate drop test described in ASTM B201 is an acceptable test method to determine the absence or presence of chromate passivation.

# Repair of Damaged Galvanized Coatings

The Quality Plan must include a procedure for repair of damaged or uncoated areas.

Prior to acceptance inspection, any uncoated areas, blisters, sharp points or other damage must be repaired in accordance with clause 4.3.1 of AS/NZS 4680.

Unless another paint system or renovation process is specified in the Contract documents (for example, where the galvanized coating is to be exposed to a highly corrosive environment), the repair paint must comply with either:

AS/NZS 3750.9 or AS/NZS 3750.15; or

APAS 0014/2, APAS 2916/1 and APAS 2908.

# Completion

Within 10 working days of the completion of each Lot, the Contractor must submit the following to the Principal:

a declaration of conformance; and

a test report that complies with the requirements of Section 5 of AS/NZS 4680 and also includes:

name of the Galvanizer and location of the facilities;

results of the Pre-galvanizing inspection (Clause 6.2);

results of the Post-galvanizing inspection, including appearance and thickness (Clause 7.2); and

details of any repairs, including location of the repair and the paint used (Clause 9).

Summary of Hold Points, Witness Points and Records

The following is a summary of the Witness Points/Hold Points that apply to this Specification and the Records that the Contractor must submit to the Principal to demonstrate compliance with this Specification.

| Clause | Hold point | Witness point | Record |
| --- | --- | --- | --- |
| 4.1 | - Commencement of galvanizing |  | Quality Plan |
| 5.6 |  | - Commencement of galvanizing of the articles |  |
| 10.1 |  |  | Declaration of conformance Test report |

Amendment Record

| Edition | Clauses amended | Action | Date |
| --- | --- | --- | --- |
| 1.0 | New specification | New | October 2023 |
| 2.0 | Clause 5 to 10 revised to accommodate the 2025 edition of AS/NZS 4680 | Various | May 2026 |

| Key |  |
| --- | --- |
| Format | Change in format |
| Substitution | Old clause removed and replaced with new clause |
| New | Insertion of new clause |
| Removed | Old clauses removed |