| AUSTROADS TECHNICAL SPECIFICATION ATS 3450 Microsurfacing |  |
| --- | --- |

Contents 1. Scope 2 2. Referenced Documents 2 3. Definitions 3 4. Quality System Requirements 4 5. Program of Work 5 6. Materials 5 Mineral aggregate 5 Mineral filler 6 Binder 6 Water 6 Additives 6 7. Mix Design 7 Responsibility for mix design 7 Mix design criteria 7 Mix design submission 7 8. Plant 8 Provision of plant and equipment 8 Paving unit calibration 8 9. Field Application 9 Placement trial 9 General 9 Cleaning 9 Protection of services and road fixtures 9 Tack coat 9 Water fog coat 10 Weather limitations 10 Rut-filling and correction 10 Production of microsurfacing mix 10 Control of traffic 11 Rolling 11 10. Sampling and Testing 11 Compliance testing 12 11. Defective Work or Materials 13 Annexure A: Summary of Hold Points, Witness Points and Records 15

# Scope

This Austroads Technical Specification ATS 3450 sets out the requirements for the manufacture and placement of microsurfacing for use on road pavements and includes requirements for the following:

component materials

properties of the microsurfacing

mix design responsibility

manufacturing and application

sampling and testing.

# Referenced Documents

The following documents are referenced in this Specification:

Australian / New Zealand Standards

AS 1141.3.1	Methods for sampling and testing aggregates: sampling: aggregates.

AS 1141.11.1 	Methods for sampling and testing aggregates: particle size distribution: sieving method.

AS 1141.12 	Methods for sampling and testing aggregates: material finer than 75 µm in aggregates (by washing).

AS 1141.22	Methods for sampling and testing aggregates: wet/dry strength variation.

AS 1141.23	Methods for sampling and testing aggregates: Los Angeles value.

AS 1141.25.2 	Methods for sampling and testing aggregates: degradation factor: coarse aggregate.

AS 1141.25.3	Methods for sampling and testing aggregates: degradation factor: fine aggregate.

AS 1141.40 	Methods for sampling and testing aggregates: polished aggregate friction value: vertical road-wheel machine.

AS 1141.41	Methods for sampling and testing aggregates: polished aggregate friction value: horizontal bed machine.

AS 1141.42	Methods for sampling and testing aggregates: pendulum friction test.

AS 1160	Bitumen emulsions for construction and maintenance of pavements.

AS 1289.3.7.1 	Methods of testing soils for engineering purposes: soil classification tests: determination of the sand equivalent of a soil using a power operated shaker.

AS 2008	Bitumen for pavements.

AS 2150	Hot mix asphalt: a guide to good practice.

AS 2341.18 	Methods of testing bituminous and related roadmaking products: determination of softening point (ring and ball method).

AS/NZS 2341.23 	Methods of testing bitumen and related roadmaking products: determination of residue from evaporation.

AS/NZS 2891.3.1 	Methods of sampling and testing asphalt binder content and aggregate grading: reflux method.

AS/NZS 2891.3.2	Methods of sampling and testing asphalt binder content and aggregate grading: centrifugal extraction method.

AS/NZS 2891.3.3 	Methods of sampling and testing asphalt binder content and aggregate grading: pressure filter methods.

AS 3582.1	Supplementary cementitious materials for use with portland and blended cements – Fly ash

Austroads

AP-C87-15	Austroads Glossary of Terms

AP-R569-18	Guidelines and Specifications for Microsurfacing

ATM 453	Surface Deviation Using a Straightedge

AGPT T221	Sampling of Bituminous Slurry.

AGPT T234	Asphalt Binder Content (Ignition Oven Method)

AGPT T250	Modified Surface Texture Depth (Pestle method).

AGPT T270	Determination of Optimum Amount of Added Water for Bituminous Slurry (Consistency Test).

AGPT T271	Determination of Set and Cure for Bituminous Slurry (Cohesion Test).

AGPT T272	Determination of Abrasion Loss of Bituminous Slurry (Wet Track Abrasion Test).

AGPT -T273 	Determination of Excess Binder in Bituminous Slurry (Loaded Wheel Test).

International Slurry Surfacing Association Standards

ISSA TB-114	Wet stripping test for cured slurry seal mix.

# Definitions

In addition to the definitions in AP-C87-15, the following definitions applies to this Specification.

| Bituminous emulsion | A system of fine droplets of bitumen with or without polymer, suspended in a mixture of water and emulsifier which begins to break on contact with surfaces and when exposed to air. |
| --- | --- |
| Microsurfacing | A bituminous slurry surfacing that contains polymer modified emulsion binder, that is capable of being spread in layers with variable thickness for rut-filling and correction courses, and for wearing course applications requiring good surface texture. |
| Polymer modified emulsion (PME) | A bituminous emulsion containing a polymer additive to assist in the development of early aggregate retention and enhanced binder and surfacing properties. The polymer additive may be added prior to, during or post emulsion manufacture to achieve specified performance attributes. |
| Principal’s Registration Scheme | Any scheme for the prequalification, registration or approval of products, manufacturers and/or suppliers in operation in the jurisdiction where the microsurfacing is to be placed. |

# Quality System Requirements

The Contractor must prepare and implement a Quality Plan that includes the documentation in Table 4.1.

Table 4.1 Quality Plan

| Clause | Description of Document |
| --- | --- |
| 6 | Details of the proposed materials and evidence that the materials comply with the requirements of this Specification, including; - details of the source of the aggregate, including evidence of that the aggregate is currently approved or registered where required under a Principal’s Registration Scheme; aggregate properties; aggregate particle size distribution; details of the filler; details of the additives; binder properties; details of water; and additive properties. |
| 7.3 | - The proposed Mix Design and supporting information (unless the Contractor proposes to use a Mix Design which has been approved or registered by the Principal in the preceding 3 years) and the manufacturer’s recommendations where appropriate. |
| 8.1 | Details of the plant to be used, including: - evidence that the equipment will perform the work as specified; evidence that all metering devices are accurately calibrated. |
| 8.4 | Procedure for the calibration of the paving unit and the component metering devices. |
| 9 | Work method statements / procedures for the production, spreading and rolling (if required in accordance with Clause 9.27) of the microsurfacing and proposed location of the joints (refer AP-R569-18). |
| 9.1 | Location and details of the placement trial (if a trial is specified). |
| 10 | Inspection and Test Plan. |

If a quarry registration or prequalification scheme for quarry products operates in the jurisdiction where the microsurfacing is to be placed, the coarse and fine aggregate (other than natural sand) must be supplied by a quarry registered or prequalified under that scheme. The current Quarry Registration / Prequalification Certificate, including its Testing Frequency Schedule (if applicable), must be included in the Quality Plan.

| HOLD POINT 1. |  |
| --- | --- |
| Process Held | Commencement of microsurfacing. |
| Submission Details | The Quality Plan must be provided to the Principal at least 10 working days prior to the commencement of work on site. |

# Program of Work

Unless specified otherwise, the Contractor must provide an overall program of work at least 2 weeks prior to the commencement of the microsurfacing works under this contract.

While the microsurfacing work is underway, the Contractor must:

- prepare a weekly update of the program and provide it to the Principal prior to the Thursday preceding the execution of the work in the following week; and

provide at least 2 weeks prior notice of any significant changes to the overall program that was submitted in accordance with Clause 5.1.

| HOLD POINT 2. |  |
| --- | --- |
| Process Held | Commencement or continuation of microsurfacing work |
| Submission Details | The overall program of microsurfacing work and weekly updates must be provided in accordance with the Clauses 5.1 and 5.2. |

# Materials

## Mineral aggregate

Mineral aggregate must consist of crushed rock or crushed gravel and may include proportions of natural sand particles.

The aggregate must be clean, hard, angular, durable and free from clay and other aggregations of fine material, soil, organic material or other deleterious material.

The aggregate must be manufactured from source rock that when crushed meets the requirements set out in Table 6.3.

Table 6.3: Aggregate properties

| Property | Limit | Test Method |
| --- | --- | --- |
| Degradation factor | 50 minimum | AS 1141.25.2 and 1141.25.3 |
| Los Angeles value | 30% maximum | AS 1141.23 |
| Wet strength | 150 kN minimum | AS 1141.22 |
| Wet/dry strength variation | 30% maximum | AS 1141.22 |
| Polished aggregate friction value | 45 minimum (1) | AS 1141.40 or AS 1141.41 and AS 1141.42 |
| Sand equivalent | 60% minimum | AS 1289.3.7.1 |

Unless a higher value is specified in the Contract documents.

When tested in accordance with AS 1141.11.1 and AS 1141.12, the aggregate (including mineral filler) must conform to the particle size distribution limits shown in Table 6.4.

Table 6.4: Particle size distribution limits for combined aggregate and mineral filler

| Sieve size (mm) | Percent passing by mass |  |  |  |
| --- | --- | --- | --- | --- |
|  | Size 4 | Size 5 | Size 7 | Size 10 |
| 13.2 | 100 | 100 | 100 | 100 |
| 9.50 | 100 | 100 | 100 | 95–100 |
| 6.70 | 100 | 100 | 85–100 | 85–90 |
| 4.75 | 90–100 | 90–100 | 70–90 | 60–85 |
| 2.36 | 65–90 | 50–70 | 45–70 | 40–60 |
| 1.18 | 45–70 | 30–50 | 28–50 | 28–45 |
| 0.6 | 30–50 | 20–35 | 19–34 | 19–34 |
| 0.3 | 18–30 | 12–25 | 12–25 | 12–25 |
| 0.15 | 10–21 | 7–18 | 7–18 | 7–18 |
| 0.075 | 5–15 | 4–10 | 5–15 | 4–8 |

## Mineral filler

Mineral filler must consist of an approved material such as Portland cement, hydrated lime or flyash with a minimum of 85% passing a 75µm sieve.

The mineral filler must be dry, free from lumps, clay, organic material and any other deleterious material and must comply in all other respects with the requirements of AS 2150. Flyash must comply with AS 3582.1 and be ‘fine grade’ in Table 1 of AS 3582.1.

The quantity of mineral filler added to the mixed materials during placement must not vary by more than 1% from the mineral filler amount prescribed in the mix design.

## Binder

Bituminous emulsions used in this process are typically proprietary grades with polymer modification so that the mix design meets the performance requirements specified in Table 7.2.

The softening point, determined in accordance with AS 2341.18, of binder recovered from the bituminous emulsion must be a minimum of 57 °C. The binder must be extracted from the bituminous emulsion in accordance with the supplier’s recommended method.

## Water

Water added to the mixture must be compatible with the component materials such that the performance requirements specified in Table 7.2 are met.

## Additives

Additives may be incorporated and nominated in a mix design provided the property limits shown in Table 7.2 are met at both extremes of the nominated additive dosage range.

The range of additive levels to be used must be stated in the mix design.

# Mix Design

## Responsibility for mix design

The Contractor is responsible for the design of the microsurfacing.

## Mix design criteria

The component materials must be proportioned such that the Consistency of the bituminous mixture meets the requirements of test method AGPT-T270. The mix design must also conform to the properties shown in Table 7.2.

Table 7.2: Mix properties

| Property | Test method | Limits |
| --- | --- | --- |
| Wear loss | AGPT -T272 |  |
|  | 1 hour soak | 540 g/m2 maximum |
|  | 6 days soak | 800 g/m2 maximum |
| Traffic time | AGPT -T271 |  |
|  | 30 minutes | 1.2 N.m minimum |
|  | 60 minutes | 2.0 N.m minimum |
| Adhesion | ISSA TB 114 | ≥ 90% |
| Excess binder content | AGPT -T273 | 540 g/m2 maximum |

## Mix design submission

Unless the Contractor proposes to use a Mix Design which has been approved or registered by the Principal in the preceding 3 years, the Contractor’s Mix Design must be included in the Quality Plan. The Mix Design must include:

- A statement detailing:

- the nominal size of the mix design;

the aggregate source, the properties of the mineral aggregate and the combined aggregate/mineral filler particle size distribution;

bituminous emulsion type and residual binder content of the mix design;

the residual binder content of the emulsion with binder properties; and

the intended proportion of each component material.

- NATA endorsed test reports demonstrating that submitted mix design complies with Table 7.2.

The proportions of the constituent materials in the Mix Design must be expressed in accordance with AGPT-T270-18.

The approval or registration of a mix design only confirms that the mix complies with the test criteria. It does not relieve the Contractor of the responsibility of supplying and placing materials which meet the compliance criteria as set out in Clause 10.

If the results of all tests submitted comply with the specified requirements, the mix design is termed the Job Mix design. The combined aggregate/mineral filler particle size distribution and the binder content of the Job Mix design are termed the Job Mix particle size distribution and the Job Mix binder content, respectively.

The Contractor's Job Mix design will be deemed to be current for a period of 3 years from the date of registration/approval, subject to the following:

- The sources and quality of the component materials in the Job Mix design remain unchanged from the approved mix design.

The proportions of the component materials in the Job Mix design remain unchanged from the approved mix design.

The mix continues to demonstrate satisfactory performance in service.

All test results included as part of the mix design submission must not be more than 12 months old at the time of submission.

# Plant

## Provision of plant and equipment

The Quality Plan must include:

- details of proposed plant and equipment and evidence that it has the capability to perform the work in accordance with this Specification; and

certificates of calibration for each metering device will not be older than 12 months at the proposed date of commencement of work on site.

All plant and equipment used in the performance of this work must be in good working condition. If the Contractor proposes to change the plant and equipment from that nominated in the Quality Plan, it must resubmit the information specified in Clause 4.1 and Hold Point 1 will reapply.

Ancillary equipment necessary for the performance of the work, such as rotary road brooms, signs, lamps, barricades, hand squeegees, shovels and hand brooms, must be provided by the Contractor and must meet all statutory requirements.

## Paving unit calibration

The Quality Plan must include a procedure for the calibration of the paving unit and the component metering devices.

Each paving unit to be used to perform the work must be calibrated with the component materials of the approved mix design prior to the commencement of construction. The certificate of calibration must not be more than 12 months old. The documentation must include an individual calibration for each component material at various settings which can be related to the paving unit's metering devices. No paving unit must be allowed to incorporate mix into the work until the calibration has been completed and/or accepted by the Principal.

| HOLD POINT 3. |  |
| --- | --- |
| Process Held | Operation using the paving unit. |
| Submission Details | If not provided with the Quality Plan, the paving unit calibration documentation with component materials of approved mix design must be provided to the Principal at least one day prior to the commencement of the micro surfacing work. |

# Field Application

## Placement trial

If specified in the Contract documents or directed by the Principal, the Contractor must undertake a placement trial prior to commencing work. The trial must use the mix, plant and personnel proposed to be used for the Works. If directed by the Principal, a separate placement trial must be undertaken for each additional nominated mix design to be used on the Works.

A placement trial may be located within the Site. The size of each placement trial must be limited to one Lot. The Contractor must design the trial to implement all the procedures described in the Quality Plan and demonstrate conformance with this Specification.

The Contractor must submit a copy of the completed Inspection and Test Plan and all relevant test results and records from the placement trial to the Principal.

| HOLD POINT 4. |  |
| --- | --- |
| Process Held | Placement of Microsurfacing. |
| Submission Details | Evidence of a successful placement trial must be provided to the Principal at least one day prior to the commencement of the remainder of the microsurfacing work. |

## General

The Contractor must notify the Principal of its proposed date for commencement of work on Site.

| WITNESS POINT 1. |  |
| --- | --- |
| Process | Commencement of Microsurfacing work |
| Notification Period | At least 5 working days before the commencement of work on Site. |

The Contractor must ensure that runoff of bituminous materials onto kerbs and shoulder does not occur.

Joints at intersections must be kept straight.

## Cleaning

Prior to any application of microsurfacing, the pavement must free of loose material, stones, dirt, dust, foreign matter and any areas of oil or fuel spillage.

## Protection of services and road fixtures

Any material used in the work must not enter or adhere to gratings, hydrants, valve boxes, manhole covers, bridge or culvert decks or other road fixtures.

## Tack coat

The Contractor must apply a tack coat if specified in the Contract documents. Where a tack coat is required, it must comprise of bituminous emulsion applied at a rate of 0.1 to 0.3 L/m2 of residual binder at 15 °C. The bituminous emulsion must be allowed to break prior to laying the microsurfacing.

## Water fog coat

The surface may be pre-wet by applying a water fog coat ahead of the spreader box. Water used for pre-wetting the surface must be applied so that the entire surface is damp but with no apparent flowing water ahead of the spreader box.

## Weather limitations

Microsurfacing must not be applied if either the pavement or air temperature is below 10 °C and falling but may be applied when both pavement and air temperatures are above 5 °C and rising Spreading must not proceed during rain or when rain appears imminent. Surfacing must not proceed where the air temperature exceeds 40 °C without consultation with the Principal and verification that the conditions will not impact on the workability and delivery of the materials.

## Rut-filling and correction

Where wheel ruts of the surface to be covered are 15 mm or more in depth, a rut-filling or correction course must be applied, prior to placing the microsurfacing. Rut-filling and correction must be carried out using a spreader box capable of laying mix across the varying cross-sectional depth such that it fills the rut and is stable.

The Contractor must nominate the number of layers of rut-filling or corrector course to be placed and the maximum thickness of microsurfacing to be applied in each layer.  In addition, the minimum time between the application of layers must also be nominated.

## Production of microsurfacing mix

The Contractor must provide sufficient information for the Principal to verify that the bituminous emulsion supplied is the same as that nominated in the mix design.

The microsurfacing must be manufactured to the Job Mix design within the maximum permitted variations specified in Table 9.15.

Table 9.15: Maximum permitted variations from Job Mix design

| Sieve size (mm) | Maximum permitted variation of aggregate particle size distribution in percent passing (by mass) |  |  |
| --- | --- | --- | --- |
|  | Sizes 4 & 5 | Size 7 | Size 10 |
| 13.2 | Nil | Nil | Nil |
| 9.50 | Nil | Nil | ± 7 |
| 6.70 | Nil | ± 7 | ± 7 |
| 4.75 | ± 7 | ± 7 | ± 7 |
| 2.36 | ± 5 | ± 5 | ± 5 |
| 1.18 | ± 5 | ± 5 | ± 5 |
| 0.6 | ± 4 | ± 4 | ± 4 |
| 0.3 | ± 4 | ± 4 | ± 4 |
| 0.15 | ± 2.5 | ± 2.5 | ± 2.5 |
| 0.075 | ± 1.5 | ± 1.5 | ± 1.5 |

- The maximum permitted variation in residual binder content must be not more than 0.5% below or 1.0% above that stated in the Job Mix design.Spreading

The mixing time must be sufficient to produce a complete and uniform coating of the aggregate and the resulting mixture must be conveyed into the moving spreader box at a rate sufficient to always maintain an ample supply across the full width of the strike-off screed.

The strike-off must be adjusted to provide an application rate which will completely fill the surface voids and provide a nominal application rate of mix.

Areas that cannot be reached with the spreader box must be surfaced using hand squeegees to provide complete and uniform coverage. Care should be exercised to leave no unsightly appearance from hand placement.

The same finish as applied by the spreader box must be provided on hand worked areas.

The surface must be smooth and true to the specified crown and grades.

Any section of paved material that is loose or broken, mixed with dirt or other impurities or is any way defective must be removed and replaced.

The longitudinal joints of the wearing course must be placed within 300 mm of either the edge or the centre of a traffic lane. The edges and joints must be lightly screeded with a hand squeegee to achieve a smooth uniform appearance and to remove excess build-up of material.

The microsurfacing must be capable of carrying slow moving vehicular traffic (< 40 km/h) within one hour of application without permanent damage occurring, such as rutting or ravelling. If this does not occur, work must cease if directed by the Principal.

All surplus microsurfacing must be removed from the site. Any aggregate stockpile sites and/or loading areas occupied for the Works must be restored to a condition similar to that which existed prior to the Contract commencing.

## Control of traffic

The Contractor must take all necessary precautions to protect the work from damage until such time as the new material has developed sufficient strength to carry normal traffic without disturbance.

Where early use of the new surface is needed to facilitate the movement of traffic, vehicles may be allowed to run on the work after initial rolling has taken place provided that vehicles are controlled to such slow speeds that no displacement of the material occurs. Where necessary, the Contractor must use patrol vehicles to ensure that traffic travels at an acceptable speed.

## Rolling

If rolling is specified in the Contract documents, the Contractor must ensure that:

- rolling occurs after the microsurfacing cures sufficiently to prevent delamination and pick-up on the roller tyres; and

it is carried out using a self-propelled pneumatic-tyred multi-wheel roller.

# Sampling and Testing

## General

The Contractor must undertake the sampling and testing specified in this Clause 10 unless specified otherwise in the Contract documents or the Principal waives any of the requirements for sampling and testing.

## Sampling

The methods, number and size of samples must be as follows:

- Three samples of mixed material from each Lot in accordance with AGPT-T221. Each sample must be a minimum of 1 kg of mixed material.

Two 2 litre samples of bituminous emulsion from each bulk delivery in accordance with AS 1160. One sample is for testing as required whilst the second sample is to be retained for reference.

Aggregates must be sampled in accordance with AS 1141.3.1.

Fillers must be sampled in accordance with AS 2150.

The Contractor must supply all equipment and facilities for sampling, including sample containers.

## Compliance testing

Compliance testing must be undertaken on a Lot by Lot basis. A Lot must not exceed the lesser of 50 m3 or one day's production

Where multiple paving units are used on a single job site, the testing frequency specified in Table 10.6 applies equally to each paving unit utilised. Where the use of continuous paving units is applied, the Contractor may submit a proposal to the Principal to decrease the testing frequencies, based on the Contractor’s ability to demonstrate consistency of material delivery.

The Contractor must ensure that testing is undertaken in accordance with Table 10.6 and provide the test results to the Principal.

Table 10.6 Test Requirements

| Verification requirement | Test Method | Minimum testing or verification frequency | Acceptance Criteria (1) |
| --- | --- | --- | --- |
| Component materials |  |  |  |
| Emulsion and residual binder | Residue from evaporation: AS/NZS 2341.23 or in accordance with the supplier’s recommended method | One for each bulk delivery of emulsion | Refer Clause 6.8 |
|  | Softening point of the residual binder: AS 2341.18 | On the first load then every 5th bulk delivery of emulsion | Refer Clause 6.9 |
| Aggregate properties | All tests specified in Clause 6. | Each mix design | Refer Clause 6 |
| Mineral filler | AS/NZS 2891.3.1, 2891.3.2 or 2891.3.3 | Producers’ compliance test report per Lot | Refer Clause 6 |
| Microsurfacing production |  |  |  |
| Particle size distribution | AS/NZS 2891.3.1, 2891.3.2 or 2891.3.3 | 2 tests per Lot | Refer Clause 9.15 |
| Residual binder content | AS/NZS 2891.3.1, 2891.3.2, 2891.3.3 or AGPT-T234 | 2 tests per Lot | Refer Clause 9.15 |
| Finished surface |  |  |  |
| Shape | ATM 453 | 5 tests per Lot or as otherwise directed by the Principal | ≤ 5 mm deviation from a 3 metre straight edge |
| Average surface texture depth in the wheel path after trafficking for one month (2) | AGPT -T250 (3) | 4 tests per Lot (4) | Sizes 4 & 5: Min 0.4 mm Sizes 7: Min 0.8 mm Sizes 10: Min 1.2 mm |

- Notes:

- Unless specified otherwise in the Contract documents.

- The texture requirements do not apply to correction courses.

The Contractor may submit a proposal to the Principal for an alternative test method to be used; however, the results must be reported as the sand patch texture depth.

The Principal may waive this requirement after the Principal and Contractor have undertaken a joint visual inspection of each Lot of completed work.

# Defective Work or Materials

For the purposes of this Clause 11, a property that does not conform to the acceptance criteria specified in Table 10.6 constitutes a defect.

A “Conforming” Lot meets all of the requirements of this Specification. Where a Lot contains 6 or less defects, that Lot is classified as a “Conditionally Conforming” Lot.

If specified in the Contract documents, the Principal may accept Conditionally Conforming work, but reduced payment, and / or additional testing requirements, will apply to that Conditionally Conforming work. Otherwise, Conditionally Conforming work must be rectified so as to comply with the requirements of this Specification.

A Lot with more than 6 defects is non-conforming and must be rectified so as to comply with the requirements of this Specification.

If the test results indicate that the defects arise from aggregate gradings and the Contractor can demonstrate by way of an alternative mix design that the gradings used have no detrimental effect on compliance with the mix properties set out in Table 7.2, the number of defects will be re-calculated based on the alternative mix design.

The cost of all replacement or correction works including any restoration work to the underlying or adjacent pavement, surface or structure must be borne by the Contractor. Material removed from the works must be replaced by conforming materials.

Calculation of defects can be based on variation of the aggregate particle size distribution and binder content from the approved mix design as shown in Table 11.7. The aggregate particle size distribution determined from samples taken on the job should be within the appropriate particle size distribution band for that nominal size. The percent passing each sieve must not vary from those specified in the approved mix design by more than the maximum permitted variation shown in Table 9.14. Any value exceeding the limits is counted towards calculation of the total number of defects. The number of defects in a Lot is determined from the average number of defects in the samples representing that Lot.

Table 11.7: Defects schedule

| Measurement | Variations | Number of defects |
| --- | --- | --- |
| % Passing | 1 or 2 measurements: 3 measurements: | 1 2 |
| 13.2 mm |  |  |
| 9.50 mm |  |  |
| 6.70 mm |  |  |
| 4.75 mm |  |  |
| 2.36 mm |  |  |
| 1.18 mm |  |  |
| 0.6 mm |  |  |
| 0.3 mm |  |  |
| 0.15 mm |  |  |
| % Passing 0.075 mm | Each increment of 0.5%: | 1 |
| Softening Point | Each 2 degrees under the minimum | 1 |
| Binder content, % mass | Each 0.25 % in excess of 1.0% over or below 0.5% under the binder content nominated in the approved mix design: | 1 |

- * Over the particle size distribution limits for the nominal size specified in Table 6.4 or the maximum permitted variations shown in Table 9.15.

If the Contractor proposes to rectify non-conforming microsurfacing by means other than removal and replacement with conforming micro surfacing, it must submit a proposal to the Principal with evidence that long term performance of the microsurfacing will not be adversely affected.

Annexure A:	Summary of Hold Points, Witness Points and Records

The following is a summary of the Witness Points / Hold Points that apply to this Specification and the Records that the Contractor must submit to the Principal to demonstrate compliance with this Specification.

| Clause | Hold point | Witness point | Record |
| --- | --- | --- | --- |
| 4.1 | - Commencement of microsurfacing |  | Quality Plan |
| 5.2 | - Commencement or continuation of microsurfacing |  | Program of work |
| 8.5 | - Operation using the paving unit. |  | Calibration Certificates |
| 9.3 | - Placement of microsurfacing (where a placement trial is specified) |  | Evidence of successful placement trial |
| 9.4 |  | 1. Commencement of microsurfacing work. |  |
| 10.6 |  |  | Test results |

Amendment Record

| Amendment no. | Clauses amended | Action | Date |
| --- | --- | --- | --- |
| - | New specification | New | December 2021 |
| 1 | Austroads test method number updated in Clause 2.1 and Table 10.6. | Substitution | February 2022 |
|  | Clause 6.7 correction to percentage variance allowed in mineral filler added to the mixed materials during placement. | Substitution |  |
|  | Clause 8.5 change of terminology in relation to the certificate of calibration. | Substitution |  |
|  | Clause 9.23 clarification of traffic type. | Substitution |  |
|  | Clause 10.4 clarification in relation to lot. | Substitution |  |
|  | Clause 10.6, new note (1) added to table. | New |  |

| Key |  |
| --- | --- |
| Format | Change in format |
| Substitution | Old clause removed and replaced with new clause |
| New | Insertion of new clause |
| Removed | Old clauses removed |

For information only. This publication does not form part of the Contract.