AUSTROADS TEST METHOD AGPT/T221

Sampling of Bituminous Slurry

Contents 1. Preface 1 2. Scope 1 3. Further Development 1 4. Safety Disclaimer 1 5. Equipment 1 6. Procedure 2 6.1 Sampling Frequency 2 6.2 Sampling Procedure 2 7. Identification of Sample 2 7.1 Records 2 7.2 Labelling 2

# Preface

This protocol was prepared by the Bituminous Surfacings Working Group (BSWG) on behalf of the Austroads Pavement Task Force (PTF).  Representatives of Austroads, the Australian Road Research Board (ARRB) and the Australian Asphalt Pavement Association (AAPA) have been involved in the development and review of this test method.

# Scope

This protocol specifies the method for sampling bituminous slurry mixture from the slurry paving unit at the paving site.

# Further Development

There are no further plans for the development of this protocol.

# Safety Disclaimer

Warning: The use of this Austroads sampling protocol may involve hazardous materials, operations and equipment.  This Austroads protocol does not purport to address the safety requirements associated with its use.  It is the responsibility of the user of this Austroads protocol to establish appropriate work health and safety practices and determine the applicability of regulatory limitations prior to use.

# Equipment

The following apparatus is required:

metal ladle capable of holding at least 1 kg of bituminous slurry

plastic sample container with water-tight lid and of sufficient capacity to contain 1 kg of sample.

- Note:	Rectangular, robust and clean plastic food containers of approximate dimensions 155 mm x 105 mm x 40 mm have been found to be suitable for collection of 1 kg samples of bituminous slurry.

# Procedure

## Sampling Frequency

Samples shall be taken near the start, middle and towards the end of the paving run so that a minimum of three 1 kg samples are collected during the run.

## Sampling Procedure

The procedure for obtaining a sample from a paving unit is as follows:

- Using a clean ladle, carefully take a sample of the bituminous slurry mixture from the outflow of the pugmill to the spreader box and immediately pour into the sample container.

- Note: The sample should be representative of the bituminous slurry coming from the pugmill.  If the sample does not appear homogenous or does not have the same appearance of the bituminous slurry coming from the pugmill, then the sample should be discarded and a new sample taken.

Place the sample container on a flat, level surface and leave it with the lid off until the bituminous slurry has set.  If required, decant residual water taking care to ensure that no binder or aggregate is lost.  Seal the sample container with the lid.

Identify sample container as per Section 7.

# Identification of Sample

## Records

For each sample record the following information:

- identification mark

- date of sampling

- type of mix and nominal size

- location of pavement site and paving run where sample was taken

- manufacturer's name

- sampling procedure used

- name of sampling operator

- sampling time (i.e. start, middle or end of run)

name and affiliation of person submitting samples.

## Labelling

Write on, or apply a sticky label to each sample container with the following information:

- sample identification mark

- number of containers in which the sample is packed

- sampling time (i.e. start, middle or end of run)

- type of mix and nominal size

name and affiliation of person submitting samples.

Note: Sample labels should be attached to the container and not the lid as the lid may be lost or swapped.

Amendment Record

| Amendment No. | Clauses amended | Action1 | Date |
| --- | --- | --- | --- |
| 1 | Commentary page Footer and header Applied revised test method number Applied new styles | New Format Format Format | June 2005 |
| 2 | Removed additional Section 3 | Removed | May 2007 |
| 3 | Applied new format Section 1: updated groups Section 4: added safety disclaimer, all subsequent sections renumbered Clause 5a Clause 6.2a note Clause 6.2b removed part of clause Section 7.1: new clauses Clause 7.2a Section 8 Reporting | Format Substitution New Substitution New Removed New Removed Removed | May 2018 |
| 1Key |  |  |  |
| Format | Change in format |  |  |
| Substitution | Old clause removed and replaced with new clause |  |  |
| New | Insertion of new clause |  |  |
| Removed | Old clauses removed |  |  |