AUSTROADS TEST METHOD ATM 112 [AGPT/T112]

Flash Point of Polymer Modified Binders

Contents 1. References 2 2. Apparatus 2 3. Procedure 2 3.1 Sample Preparation 2 3.2 Determination of Flash Point 2 4. Reporting 3 5. Precision 3 Amendment Record 4

Commentary

Preface

This test method was prepared by the Bituminous Surfacings Working Group (BSWG) on behalf of the Austroads Pavements Task Force (PTF). Representatives of Austroads, the Australian Road Research Board (ARRB) and the Australian Asphalt Pavement Association (AAPA) have been involved in the development and review of this test method.

This test method is intended to indicate fire risk and the presence of volatile oils in polymer modified binders (PMBs). Minimum flash points are specified to minimise the risk of flammable vapours accumulating in the ullage space of transport and storage containers with consequent risk of explosion.

The flash point of a binder is determined by slowly heating the material in an open metal cup until a temperature is reached at which vapours on the surface of the material are ignited or ‘flash’ in the presence of a test flame.

Scope

This test method sets out the procedure for the determination of the flash point of PMBs. This test method is applicable to PMBs used in the construction and maintenance of pavements (as specified in ATS 3110).

Further Development

There are no further plans for the development of this test method.

Safety Disclaimer

Warning: The use of this Austroads test method may involve hazardous materials, operations and equipment. This Austroads test method does not purport to address the safety issues associated with its use. It is the responsibility of the user of this Austroads test method to establish appropriate work health and safety practices and determine the applicability of regulatory limitations prior to use.

# References

The following documents are referred to in this method:

| Austroads Test Methods |  |
| --- | --- |
| ATM 101 | Method of sampling polymer modified binders, polymers and crumb rubber. |
| ATM 102 | Protocol for handling modified binders in preparation for laboratory testing. |
| ATS 3110 | Supply of polymer modified binders. |
| Australian/New Zealand Standards |  |
| AS/NZS 2341.1 | Methods of testing bitumen and related roadmaking products, Part 1: Precision data - Definitions. |
| AS 2341.14 | Methods of testing bitumen and related roadmaking products, Method 14: Determination of flashpoint of bitumen |
| ASTM International |  |
| ASTM D92 | Standard test method for flash and fire points by Cleveland open cup tester. |

# Apparatus

- The required apparatus is given in AS 2341.14 or ASTM D92.

- If AS 2341.14 is used to determine flash point, then other thermometric devices may be used to measure temperature provided that their accuracy, precision and sensitivity are equal to or better than the thermometer prescribed in AS 2341.14.

# Procedure

## Sample Preparation

Samples for testing shall be provided in accordance with ATM 101 and ATM 102.

## Determination of Flash Point

- Determine the flash point of the binder in accordance with the method set out in AS 2341.14 or ASTM D92.

- If AS 2341.14 is used to determine flash point then the thermometer may be replaced by another type of thermometric device which meets the requirements of Section 2(b).

- If ASTM D92 is used to determine flash point, round the corrected flash point result to the nearest 10°C.

# Reporting

Report the flash point result, in °C, to the nearest 10°C.

# Precision

The following criteria should be used for judging the acceptability of results with 95% probability (see AS/NZS 2341.1) using flash point results which are obtained using AS 2341.14 or ASTM D92 which are rounded to the nearest 1°C:

- Repeatability: Duplicate flash point determinations by the same operator using the same equipment shall not be considered suspect unless they differ by more than 8°C.

- Reproducibility: Flash point determinations submitted by each of two laboratories shall not be considered suspect unless they differ by more than 18°C.

Amendment Record

| Amendment No. | Clauses amended | Action1 | Date |
| --- | --- | --- | --- |
| 1 | Commentary Page Footer and header Applied revised test method number Applied new styles | New Format Format Format | June 2005 |
| 2 | New test method number applied | Substitution | March 2006 |
| 3 | Foreword | Removed | February 2020 |
|  | Safety Disclaimer | New |  |
|  | Safety precaution statement | Removed |  |
|  | References | Substitution |  |
|  | Apparatus/Procedure – allows both AS 2341.14 and ASTM D92 to be used to perform the test. Allows an equivalent thermometric device to be used with AS 2341.14 in addition to the specified thermometer | Substitution |  |
|  | Reporting – flash point results now rounded to the nearest 10 °C to be consistent with AS 2341.14 | Substitution |  |
|  | Precision statements included | New |  |
| 4 | New test method number applied | Substitution | July 2022 |
|  | References updated | Substitution |  |

| 1Key |  |
| --- | --- |
| Format | Change in format |
| Substitution | Old clause removed and replaced with new clause |
| New | Insertion of new clause |
| Removed | Old clauses removed |